## Slide 1: EC CAST Final Symposium: Analytical techniques and their application
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
B. Z. Cvetković1, E. Wieland1, D. Kunz1, J. Tits1, G. Salazar2, S. Szidat2 1Paul Scherrer Institut, 2University of Bern
16th January 2018

## Slide 2
Outline
2
PSI - Laboratory for Waste Management CAST Symposium 2018
Introduction
PSI contribution to CAST
Experimental procedure and setup
Results: Corrosion experiment
  Analysis of dissolved species
  Analysis of gaseous species
Conclusion and outlook
Notes: to separate single organic compounds

## Slide 3
Repository
Geosphere
Soil
14C
14C
Disposal of low- and intermediate level radioactive waste
Cementitious materials are used for conditioning the waste and the construction of the engineered barrier system (container, backfill, etc.)
Container
(concrete,
mortar, steel)
Alkaline & reducing conditions
Cavern backfill
(porous mortar)
Waste package
(cement & steel)
Mortar
Mortar
Construction
concrete
Shotcrete
liner
Host Rock
Deep geological disposal of radioactive waste
3
PSI - Laboratory for Waste Management CAST Symposium 2018
Notes: (container, backfill material, liner)

## Slide 4
Corrosion experiment with activated steel
Chromatographic separation and sample preparation using gas chromatography (GC) or ion chromatography (IC) to separate single organic compounds
14C accelerator mass spectrometry (AMS) used to determine 14C activity
PSI contribution to «CAST» WP 2
4
PSI - Laboratory for Waste Management CAST Symposium 2018
Notes: to separate single organic compounds

## Slide 5
Hydrocarbons: Methane, Ethane, Ethene, Propane, Propene, Butane
Carboxylic acids: Formic acid, Acetic Acid, Oxalic acid, (Malonic acid, Lactic acid)
Alcohols, aldehydes: Methanol, Ethanol, Formaldehyde, Acetaldehyde, Propionaldehyde
Identical carbon speciation for two different iron powders
Experimental parameters:
  Pre-cleaned commercial iron powder
  Artificial porewater solutions (pH 12.5)
Limited number of species: Max. 20 species, but different classes of target compounds
Experimental procedure - Target compounds
5
PSI - Laboratory for Waste Management CAST Symposium 2018
Notes: What does this mean? Confirmation of ox+red species along with findings from literature + analytical procedure works
time-dependent concentrations
[Deng 1997, Agrawal 2002, Seewald 2001, Yamaguchi 1999, Kani 2009]

## Slide 6
Activated steel sample from NPP
  Small sample, but high dose rate (60Co)
  Use of hot cell not possible (no space for corrosion reactor inside available hot cell)
Activated steel sample has a low 14C content
  1.78·104 Bq/g ( 0.1 µg 14C/g)
Very low corrosion rate of steel under alkaline conditions
  Rate  50 nm/year
Expected concentration
Experimental set-up: (2 g Fe, surface area of 2 cm2/g, 300 mL reactor volume, 1 day reaction time)
5.610-15 mol 14C/(Ld) (total 14C) = 7.810-14 g 14C/(Ld) (total 14C) = 1.28 µBq 14C/(Ld) (total 14C)
Analytics: small volumes, chromatographic separation (speciation) → additional dilution
Development of compound-specific 14C analysis as a combination of chromatographic separation of organics and 14C AMS detection:
14C accelerator mass spectrometry (AMS): ~ 10-18 g 14C (= 20’000 atoms)
(20 µg total 12,13C carbon, 14C/12,13C isotopic ratio)
Experimental procedure - Analytical challenges
6
PSI - Laboratory for Waste Management CAST Symposium 2018
Notes: -15 -> femto
-18 -> atto
Challenge - Very low concentrations of 14C bearing compounds expected
4*10E-14 = 0.14 fm (20ug 12C) = 0.06 uBq/uL

## Slide 7
β− counting
− Large sample amounts
− Long measurement time
− Background
AMS (graphite targets)
− Small sample amounts
− Fast measurements
− Isobar suppression
− Molecule break-up
Direct gas measurement with AMS
− Ultra small sample amounts
− Hyphenation possible
Sample size
12C 14C
1 g
1 mg
10 µg
10’000 µBq
10 µBq
0.1 µBq
β- spectrometry: Counting of disintegrating atoms (LSC) [14C: s-1]
Accelerator mass spectrometry (AMS): Counting of stable atoms [14C/(12C ·1.18·10-12)]
Fraction modern: 1 fm: 1 F14C = 14C/(12C · 1.18 ·10-12)
Experimental procedure - Carbon-14 analysis
7
PSI - Laboratory for Waste Management CAST Symposium 2018
Notes: Nachweisgrenze in Bq für b-counting und large AMS nach Verdünnung mit fossilem Material bei 5 pMC
Nachweisgrenze für small AMS für 1 µgC und 100 pMC (Unsicherheit für diese Messung: 5%).
Decay counting

## Slide 8
Gas-tight reactor (pressure autoclave) for the corrosion experiments with specimens prepared from activated steel nut
Features
- Combined stirring and sample container for steel nut, PEEK liner
- Sampling of liquid and gas phase and replacement of liquid phase without opening the reactor
- Pressure control and measurement of O2 concentration and temperature in aqueous phas
8
PSI - Laboratory for Waste Management CAST Symposium 2018
Experimental procedure - Corrosion reactor

## Slide 9
Time | O2 | Pressure | TO14C-AMS |  | TOC | Hydrocarbons [µM] |  |  | Carboxylic acids [µM] |  |  |  |  | Co-60
[d] | [ppb] | [bar] | [F14C] | [Bq/L] | [ppm] | Methane | Ethane | Ethene | Formate | Acetate | Oxalate | Glycolate | Lactate | [Bq/mL]
0 | 58.8 | 5.03 | 0.00 | 0.00 | - | - | - | - | < 5 | n.d. | < 0.1 | n.d. | n.d. | -
1 | 43.2 | 5.15 | 0.10 | 0.04 | - | n.d. | n.d. | n.d. | 7 | n.d. | 0.3 | 0.4 | n.d. | -
15 | 38.9 | 5.02 | 0.99 | 0.45 | 2.44 | n.d. | n.d. | n.d. | 8 | n.d. | 0.5 | 1.3 | 1.6 | -
29 | 37.5 | 5.04 | 1.56 | 0.70 | 2.60 | 0.07 | n.d. | n.d. | 7 | n.d. | 0.5 | 1.4 | 1.2 | 5.2
93 | 43.2 | 5.06 | 3.53 | 1.60 | 4.67 | 0.42 | n.d. | n.d. | 13 | < 5 | 0.7 | 1.7 | 2.8 | 5.2
286 | 59.7 | 5.19 | 2.94 | 1.33 | 6.18 | 0.55 | 0.05 | 0.02 | 49 | 21 | 0.3 | 1.6 | 2.5 | 4.4
412 | 69.5 | 5.02 | 1.46 | 0.66 | 6.57 | 0.99 | 0.02 | 0.06 | 20 | 10 | 1.0 | 1.3 | 4.1 | 3.3
“Hot” experiment with two activated steel nut segments:
14C-AMS TOC GC-MS IC-MS
γ
Corrosion experiment: Results after 412 days
    Fast initial corrosion till 100 days followed by slow corrosion
    Corrosion seems slower than expected
    Single 14C-fractions not detectable (dilution due to separation)
    Pre-concentration required!
9
PSI - Laboratory for Waste Management CAST Symposium 2018

## Slide 10
TO14C
sample
3x
IC injection
Acetate + Formate + Oxalate + Malonate
A B C
Freeze drying - 1
A*
A*
A*
3x 500 µL → 3x 100 µL
5x pre-concentration
Freeze drying - 2
A B C
A B C
A B C
300 µL → 60 µL
5x pre-concentration
A*
A**
A**
A**
A**
25x pre-concentration
      2x freeze drying → 25x 0.01 Bq/L = 0.25 Bq/L per fraction
      1 Bq/L TO14C, two main fraction = 0.5 Bq/L, dilution of 1/50 → 0.01 Bq/L
      LOD = 0.027 Bq/L LOQ = 0.12 Bq/L
    Pre-concentration required
10
PSI - Laboratory for Waste Management CAST Symposium 2018
Corrosion experiment: Dissolved species
Freeze drying process
Notes: Max 45 Bq/L

## Slide 11
Measurement of single fractions after 412 days
Fraction* | Concentration |  | Dilution corrected concentration | 
 | [Bq/L] | Error | [Bq/L] | Error
LA | < 0.004 | 0.001 | < 0.20 | 0.04
FA | 0.007 | 0.001 | 0.31 | 0.03
AA | 0.007 | 0.002 | 0.24 | 0.08
LA + FA + AA = TO14C | - | - | 0.74 | 0.15
*MA and OA fraction were not measured in this experiment
Procedure:
- 9x injection of the TO14C sample (triplicates A+B+C)
- Collection of lactic (LA), formic (FA) and acetic acid (AA)
- MQ samples as procedure background
- Subsequent freeze drying process
→ Triplicates of each fraction
→ Pre-concentration factor of 15 ± 7x
Measurement of single fraction is enabled by pre-concentration
TO14C (0.74 Bq/L) fractions = 112 ± 23% of TO14C (0.66 Bq/L)
AA, FA and LA are main dissolved organic corrosion products
11
PSI - Laboratory for Waste Management CAST Symposium 2018
Corrosion experiment: Dissolved species
Notes: BG = 0.07 LOQ 0.005 Bq/L
→ Cross contamination during drying process?

## Slide 12
Liquid sample handling, separation and detection
Liquid samples separated and measured with AMS 
First test with activated steel sample combined with IC-AMS 
Corrosion experiment with activated steel
Installation of reactor and sampling system completed 
“Cold” test experiments with reactor system 
“Hot” corrosion experiment (started May 2016) & final development of methods 
  Sampling of liquid and gas phase (C-12 and C-14 analysis) ongoing ()
  Pre-concentration method for analysis of single fraction 
  AMS-Method for analysis of total inorganic carbon-14 (TI14C) 
Summary: Reactor and dissolved species
12
PSI - Laboratory for Waste Management CAST Symposium 2018

## Slide 13
Development of the sampling system for gas samples
Schematic representation of the setup:
Second separation column enables separation
of hydrocarbons (CnH2n+2) and CO2
TCD does not distinguish between hydrocarbons (CnH2n+2) and CO2
    Final approach: Splitless injection with direct 12C addition through a second injection loop (“carrier” & “internal standard”)
13
PSI - Laboratory for Waste Management CAST Symposium 2018

## Slide 14
Gas sample handling, separation and detection
Installation and optimization of GC/MS and oxidation reactor 
Capacity tests of column, TCD and oxidation oven 
Separation of methane and CO2 with second separation column 
Fraction collection system
Definition of the requirements (e.g. number and sizes of the collection loops) 
Installation and testing of the system 
  Minor bug fixes in collection software ongoing ()
Recovery test with fossil and modern methane ongoing ()
Gas samples from the corrosion experiment (samples available)
  Single fractions (14C-methane) next step
  Total carbon-14 (T14Cgas ) next step
14
PSI - Laboratory for Waste Management CAST Symposium 2018
Summary: Gaseous species

## Slide 15
Conclusions
15
PSI - Laboratory for Waste Management CAST Symposium 2018
Activated steel
Dissolved organic 14C
Speciation determined
Main fractions (AA, FA, LA)
Gaseous 14C
Method developed
Speciation ???
Inorganic 14C
Method developed
First measurements

## Slide 16
Scientific and technical support
Paul Scherrer Institut: Dr. J. Tits, D. Kunz, R. Brütsch
University of Bern (Switzerland): PD Dr. S. Szidat and Dr. G. Salazar
Brechbühler AG, Schlieren (Switzerland): Ph. Mottay, P. Pichler, B. Oberlin
Financial support
swissnuclear
National Cooperative for the Disposal of Radioactive Waste (Nagra), Switzerland
7th EU Framework project "CAST" (Carbon Source Term)
Acknowledgements
16
PSI - Laboratory for Waste Management CAST Symposium 2018

## Slide 17
Thank you for your attention!
Notes: Beispiel um die Schlussfolie als Danksagung zu nutzen

## Slide 18: LARA: Laboratory for the Analysis of 14C with AMS at University of Bern
MICADAS: Mini Carbon Dating System
Experimental procedure – Carbon-14 analysis
2 mass spectrometer
Low energy side (negative ions) + high energy (positive ions) after the accelerator
2 filter to remove isobars of 14C (12CH2, 14N)
(Laboratory for Environmental and Radiochemistry; PD Dr. S. Szidat)
18
PSI - Laboratory for Waste Management CAST Symposium 2018
Notes: AMS: Only bulk analysis (in spite of MS separation)
Filters isobars 12CH2