## Slide 1: CArbon-14 Source Term CAST
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Name: Michel Herm
Organisation: KIT-INE
Date: 16.01.2018

## Slide 2: Formation of 14C in nuclear reactors
Physical formation of 14C in fuel assemblies by
  neutron capture reactions.
  ternary fission in the fuel.
  during reactor operation.
ternary fission in LWR fuel
1.7×10−6 per thermal 235U fission 1.8×10−6 per thermal 239Pu fission

## Slide 3: Formation of 14C in nuclear reactors
N and C are present as impurities in steel but also in Zircaloy cladding and nuclear fuel.
17O is a stable low-abundance, naturally occurring isotope (e.g. water coolant, corrosion layers).
Great uncertainty of nitrogen content in stainless steel (≤ 0.11 wt.% according to DIN EN 10088-3).

## Slide 4: 14C inventory calculations
 | Study performed by KIT within CAST (stainless steel plenum spring) |  | Schumann et al. 2014 (guide tube nut)
Model | MCNP model of fuel assembly | SCALE/TRITON model of fuel assembly | MCNP reactor model of Gösgen PWR
Activation | CINDER | ORIGEN-S | GRS-AKTIV2
N impurity [wt.%] | 0.008 | 0.008 | 0.0112 ± 0.0031
Experimental 14C inventory [Bq/g] | 2.7(±0.3)×105 |  | 17.8(±2)×103
Calculated 14C inventory [Bq/g] | 8.5×104 | 9.5×104 | 4.5×103
Ratio E/C | ~3.2 | ~2.8 | ~4

## Slide 5: 14C inventory calculations
Good agreement between MCNP/CINDER and SCALE/TRITON/ORIGEN-S calculations performed by KIT and NAGRA.  assumption of 0.008 wt.% N impurity in stainless steel is too low.
Schumann et al. 2014 experimentally determined N content in non-irradiated steel sample.  application of MCNP “reactor model” on activation of small components inside a reactor is limited (local neutron flux).
Simulation of local neutron flux around sample and knowledge of N content is important for accurate 14C inventory calculations.

## Slide 6: Status of 14C in steel
N, C in stainless steel before irradiation is potentially present as
  interstitial solid solution.
  N also present as nitrides of alloying metals.
  C also present as metal carbides.
  carbonitrides maybe also form.
After formation, highly excited, and charged 14C competes with available reactants to form carbides, carbonitrides or oxides (interstitial 14C from interstitial N).
Chemical state of 14C is far from clear in stainless steel.

## Slide 7: Status of 14C in steel
Carbides:
  Salt-like carbides (Al4C3, CaC2, Mg2C)  decompose to methane, acetylene.
  Transition metal carbides (Cr, Mn, Fe, Co, and Ni carbides are hydrolysed by dilute acids and water to hydrogen and hydrocarbons).
  Interstitial compounds of group 4, 5, and 6 (e.g. ZrC, WC).
  Covalent compounds (boron or silicon carbides).
Carbonitrides:
  Less reactive than carbides. However, reactivity increases with ratio C:N.
Oxides:
  Oxygen present in corrosion layers on metal surfaces.
  Within oxide layer, 14C possibly present as sorbed species (originating from coolant) or directly formed in layer (carbide, oxide).
reactivity

## Slide 8: Status of 14C in steel
Carbides:
  Formation of Fe, Ni, Mn, and Cr carbides in steels is possible according to standard free energy of formation Gf at T range of reactor water coolant.
  Formation of carbides with minor alloy components and trace impurities must be also taken into account.
  Nb, Mo, and Cr carbides require much higher formation T than expected from water coolant of light water reactors.
  Fe3C is known to be present in steels.

## Slide 9: Status of 14C in steel
Oxides:
  Formation of oxide–carbon species in steels.  free energy of formation with respect to oxygen potential must be analysed.
  Oxidation only possible in specific T range.
  Gf of CO2 almost T independent stability of CO increases with T (Boudouard reaction).
  Fe, Mn, Mo, Zr, etc. significantly lower Gf values compared to oxidation reactions of C, except Ni.
  No driving force to form CO or CO2 compounds in indicated T range.
surface T of cladding during reactor operation

## Slide 10: Summary and conclusions
Local neutron flux around sample in reactor and N content in steel are key parameters for accurate 14C inventory calculations.
C and N predominantly uniformly distributed solid solution in stainless steels.
Formation of Fe, Ni, Mn, and Cr carbides in steels is possible according to standard free energy of formation Gf at T range of reactor water coolant.
Thermodynamic data show almost no driving force to form CO or CO2 compounds after formation of 14C atom. In the T range of 500 to 550 K only NiO could release oxygen to form CO2.
Chemical form of 14C in irradiated steels may be different from bulk.

## Slide 11: Acknowledgments
M. Böttle | V. Metz
E. Bohnert | N. Müller
R. Dagan (INR) | INE workshop
E. González-Robles | INE infrastructure team
B. Kienzler | 
P. D. W. Bottomley | R. Nasyrow
R. Gretter | D. H. Wegen
S. Caruso | 
Funding:
Thank you for your attention!
The research leading to these results has received funding from the European Union’s European Atomic Energy Community’s (Euratom) Seventh Framework Programme FP7/2007-2013 under grant agreement no. 604779, the CAST project.