## Slide 1
Laurent Charlet , BinMa, Alex Fernandez Martinez
ISTerre, University of Grenoble Alps et ESR
Jean Charles Robinet , Benoit Madé
ANDRA, Chatenay Malabry, France
FUNDING:
Possible Fate of inorganic carbon-14 releaseD from activated steels under conditions of a geological repository

## Slide 2
Recognition of the principal RN oxyanions (including for 13C carbonate
and selenite structural “analogue”) “retardation” processes
Knowledge of the most important mechanisms that govern RNs in near field
Particular role of calcite and concrete DLHs in these processes
Distinguish how local redox potential, dictated by iron corrosion,
impacts this retardation
Confrontation of these observed mechanisms with 14C release
and transfer observation
Goals of this Presentation
Notes: Other acknowledgements as appropriate in the presentation.

## Slide 3
Reactivity of calcite towards Selenite and 13C carbonate
Reactivity of 12C calcite towards 13C carbonate
Co-precipitation of Selenite (a carbonate analogue) into calcite
Reactivity of carbonate to Fe corrosion products
Outline
Immobilization of the redox-sensitive RNs in cement layered double hydroxides (LDHs)
Speciation of redox sensitive RNs (e.g., SeIV, MoVI.. And CIV)
Sorption mechanisms on Afm and impacton RN fate
Redox processes at iron/steel interface
Redox active couples (Sb, Se, Mo, U)
Equilibration within NZVI/CPW suspension and XANES measurements
In situ measurement of Eh
Implication for the fate/speciation of 14C?
Notes: Other acknowledgements as appropriate in the presentation.

## Slide 4
Calcite reactivity towards 13CO32- and selenite (SeO32-)
13C reaction with 12C calcite
Long term kinetic experiment
Kinetic model
Selenite ion reaction with calcite
Wet chemistry
Neutron Diffraction experiments
EXAFS spectroscopy
WASP theoretical chemistry model
Notes: Other acknowledgements as appropriate in the presentation.

## Slide 5
Modified from Charlet and Manceau (1993), Banfield and Nealson (1997)
Selenite or Carbonate ion sorption on mineral particle
  Structural:
  Co-precipitation
  Surface:
  Outer-sphere complex
  Inner-sphere Complex
Easily exchangeable
Or
Specifically adsorbed
“Immobilized” by
Diffusion and/or
coprecipitation
Se
e.g. Se(IV)
Se
Se
Se
Se (co)precipitation
Ca(CO3,SeO3))
Se
Se
Se
Se
Mineral (e.g. clay, FeOOH or calcite)
Notes: Each of these processes may be affected by pH and Eh change.
Dissolution
Desorption
Arsenic different to most contaminants – oxyanions – never mono atomic cations.
Physisorption; b) chemisorption; c) detachment; d) absorption or inclusion (impurity ion that has a size and charge similar to those of one of the ions in the crystal); e) occlusion (pockets of impurity that are literally trapped inside the growing crystal); f) attachment; g) hetero-nucleation (epitaxial growth); h) organo-mineral complexation; i) complexation to bacterial exopolymer.

## Slide 6
Water pre-equilibrated with standard
calcite and air, reacted with suspension of
Filtered sample analyzed
for d13C by IR-CRDs
Replacement of 12CO32- by 13CO32- in calcite
Diffusion of 13C into pure 12C calcite
Pure 12CaCO3
(CaO + 12CO2)

## Slide 7
Diffusion of 13C into pure 12C calcite
21 °C
50 °C
Surface adsorption
Followed by
Solid diffusion
Vs.
Oswald Ripening

## Slide 8
Assumptions for an Ostwald ripening model
The synthesis creates a size distribution of calcite cubes of side L and single-particle area A0
Solubility is dependent on the surface free energy, g, and L
Coarsening will transfer material from small to larger particles
The newly grown material will have same isotope ratio as solution
Smaller particles dissolve
Larger particles grow, adding 13C at same isotopic ratio as solution
Critical size threshold
Cross-section through coarsened particle
Use solution C isotope ratio from Gehin et al.
13C:12C = 1/(89.7949-1) = 0.0113
13C:12C = 0.0113
13C:12C = 0

## Slide 9
Minerals: Replacement of CO32- by SeO32- in calcite
Minerals: replacement of SO42- by SeO42- in gypsum
Coprecipitation due to structural similarities
selenite vs. selenate
carbonate vs. sulfate
Carbonate Selenite
Se(IV) Se(VI)

## Slide 10
Coprecipitation: Se (IV) substitution for carbonate in calcite
Hypothesis...
Replacement of CO32- by SeO32-
Method:
Ab-initio simulations (VASP)
starting from “flat” SeO32-
obtained unit cell expansion of
the Se-rich calcite unit cell
confronted to:
Neutron diffraction data
Input to model EXAFS data
  Aurelio et al. Chem. Geol, 2009

## Slide 11
Selenite (SeO32-) substitution for Carbonate within calcite
  Aurelio et al. Chem. Geol, 2009

## Slide 12
Coprecipitation of Se in calcite (CaCO3)
with Selenite (SeO32-) ions substituting for carbonate ions
  Aurelio et al. Chem. Geol, 2009
  Fernandez-Hernandez et al., 2011
Theoretical ab-initio simulations of the crystallographic structure using Vienna Ab initio simulation package (VASP) vs. Neutron diffraction and EXAFS spectroscopy

## Slide 13
Natural nanoparticles abundant in the environment!
Sorption of CO2 on goethite/ferrihydrite in 0.1 M NaNO3 Double-layer surface complexation model with standard site density and surface pKa
Carbonate adsorption on Steel corrosion products
CO2, thus inorganic 14C, do adsorb on Steel corrosion products
Appelo et al., EST, 2002
SEM image
SEM
Notes: Other acknowledgements as appropriate in the presentation.

## Slide 14: Contrasted sorption on calcite, clays and Fe oxyhydroxides
Strong
Inner sphere complexes
Calcite, Fe Oxyhydroxydes
with Se(VI) & Se(IV)
Mineral
Weak
Outer sphere complexes
Clays (e.g. kaolinite)
with Se(VI)
Fernandez Martinez and Charlet 2009
Hayes et al., 1987

## Slide 15
Redox Barrier: Steel in reinforced concrete

## Slide 16
Strategy for Eh determination

## Slide 17
Steel cross-section (sandwich model)
RNs | Kd-mean m3 kg-1 | Kd-min m3 kg-1 | Kd-max m3 kg-1
U(VI) | 2 | 0.4 | 10
Se(IV) | 0.2 | 0.01 | 6
Mo(VI) | 3.0×10-3 | 3.0×10-4 | 3.0×10-2
Sb(V) | 20 | - | -
Reactions and Eh equations between the redox sensors.
Redox Couple Half-Reaction | Equation
UO22+(aq) + 2e- = UO2(s) | Eh = Eh0 – 0.03log(1/[UO22+])
MoO42-(aq) + 4H+ + 2e- = MoO2(s) + 2H2O | Eh = Eh0 – 0.03log(1/[MoO42-]·[H+]4)
SeO32-(aq) + 6H+ + 4e- = Se0(s) + 3H2O | Eh = Eh0 – 0.015log(1/[SeO32-]·[H+]6)
2Sb(OH)6-(aq) + 4H+ + 2e- = Sb2O4(s) + 8H2O | Eh = Eh0 – 0.03log(1/[Sb(OH)6-]2·[H+]4)
Distribution coefficient of hydrated cement for varying RNs.a
a From ANDRA
Sorption on steel (redox)
Sorption in concrete
From core to surface
Fe-FeO/Fe3O4/Fe2O3
Various redox-active couples
Notes: The passivation layer of steel in concrete can be considered as
a magnetite-based structure with an inner level that is richer in
Fe2+ and an outer level that is richer in Fe3+ species [59]. This
structure is dynamic with varying borders between the stoichiometries
FeO/Fe3O4/Fe2O3 that mainly depend on the
oxygen availability.
The data from a range of techniques are considered to indicate a two layer film(sandwich model) with an Fe(II) oxide adjacent to the metal and an Fe(III) oxide making up the outer layer.

## Slide 18
Spectroscopy based EH computation
EH obtained by the Nersnt equation for 3 RNs (Se, U, Sb) and various Fe corrosion product couples in CPW
Assuming:
The ICP measured total aqueous concentration in CPW is used to compute the activity of the dominant oxidized species
The reduced species (and thus the half reaction equation) given by the dominant solid species, as determined by HE-XRD (with PDF analysis; left), XANES (center: Se) or XPS (left: U) spectroscopy
m Aox + n H+ + e  p Ared + q H2O

## Slide 19
Half redox reactions for various redox-active couples

## Slide 20
Result: EH imposed by steel (various Fe couples) in CPW

## Slide 21
Implications for CAST
Disproportionation redox reaction
C(O) = HCO3- + CH4(g) + H+ (or organic C ? )
How these Eh in-situ estimate could be used to understand 14C fate?
pe = -7.5 ± 1.1 (Eh= -450 ± 70 mV and
pH =13.5 Eh(in Volts) = pe 0.059)
The Eh of steel (iron) in contact with CPW
is far above stability domains of organic C compounds
Wieland and Hummel, 2015
Notes: Other acknowledgements as appropriate in the presentation.

## Slide 22
AFm-Cl2 (Ca4Al2(OH)12·Cl2·nH2O)
Portland cement composition
C3A +
gypsum
AFm-SO4 (Ca4Al2(OH)12·SO4·nH2O)
Aluminum calcium monosulfate
AFm
Immobilization of the redox-sensitive RNs
in cement layered double hydroxides (LDHs)
Notes: Generally, Portland cement is used to make the concrete cask and is composed of these common phases, including gypsum. As we all know, the C represents CaO, S SiO2, A Al2O3, and F is Fe2O3. Gypsum plays a very important role in controlling the hardening rate of the cement. Upon the cooling of clinker, a small amount of gypsum is introduced during the final grinding process, to slow down the “setting of cement”. On the other hand, each type of Portland cement contains C3A phases. Hydration of C3A is fastest and also generates most heat which will react with gypsum and mainly form AFm and ettringite phases. The AFm phases are layered double hydroxides. Its crystalline layer structure is derived from that of portlandite, but with one third of Al replacement. The resulting charge imbalance gives the layers a positive charge which is compensated by intercalated anions, e.g., SO42-, Cl-, OH-, etc. Its general formula is like this, where X represents one divalent or two monovalent interlayer anion. Generally, the inter-layer anions’ bonding are relatively weak, and this gives AFms remarkable ability to remove anionic contaminants. Two AFm phases were synthesized and they have different sizes and the same specific hexagon shape. The objective of this project is to evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-.
During the cement manufacturing process,

## Slide 23
Do MoO42- and SeO42- sorb, like I-,
and thus have retardation impact?
Aimoz et al, EST, 2012
Ca4Al2(OH)12· X ·(2−6)H2O
X: SO42- , 2Cl-
Anions: MoO42- , SeO32-
To evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-

## Slide 24
with increasing [MoO42-]initial : ~1 µM to ~5 mM
Modeling batch sorption isotherms
Sorbed vs. Aqueous amount
Ma et al, ES&T2017
Ma et al., ES&T, 2017
Notes: Generally, Portland cement is used to make the concrete cask and is composed of common phases, including gypsum, where C represents CaO, S SiO2, A Al2O3, and F is Fe2O3. Gypsum plays a very important role in controlling the hardening rate of the cement. Upon clinker cooling, a small amount of gypsum is introduced during the final grinding process, to slow down the “setting of cement”. On the other hand, each type of Portland cement contains C3A phases. Hydration of C3A is fastest and also generates most heat which will react with gypsum and mainly form AFm and ettringite phases. The AFm phases are layered double hydroxides. Its crystalline layer structure is derived from that of portlandite, but with one third of Al substitution by Ca. The resulting charge imbalance gives the layers a positive charge which is compensated by intercalated anions, e.g., SO42-, Cl-, OH-, etc. In the general formula, X represents one divalent or two monovalent interlayer anion. Generally, the inter-layer anions’ bonding are relatively weak, and this gives AFms remarkable ability to remove anionic contaminants. Two AFm phases were synthesized and they have different sizes and the same specific hexagon shape. The objective of this project is to evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-.
Batch experiment was conducted as a function of initial anionic concentration. Logarithms of removed molybdate amount and final aqueous anion concentration are plotted in Fig. 1. The data at low loading can be interpreted by Langmuir adsorption isotherms. And the dot lines of each sorption stage indicate the theoretical sorption capacities. When adding more Mo into the AFm system, the sorption process will go through anion exchange and Ca-precipitation meachnisms as the increasing coverage. From the aqueous results, AFm-Cl2 phase has a much stronger affinity and larger adsorption capacity for molybdate than AFm-SO4. For AFm-Cl2, above 95% molybdate was removed within 48 h, meantime, proportional inter-layer Cl- was released. The larger sorption capacity may result from the smaller size and more exchangeable intercalated anion.
The sorption products of reactor A-F were selected to be characterized by in-situ XRD and XAS.

## Slide 25
Edge sorption: Mo as a molecular probe
Ma et al., ES&T, 2017
Notes: Generally, Portland cement is used to make the concrete cask and is composed of common phases, including gypsum, where C represents CaO, S SiO2, A Al2O3, and F is Fe2O3. Gypsum plays a very important role in controlling the hardening rate of the cement. Upon clinker cooling, a small amount of gypsum is introduced during the final grinding process, to slow down the “setting of cement”. On the other hand, each type of Portland cement contains C3A phases. Hydration of C3A is fastest and also generates most heat which will react with gypsum and mainly form AFm and ettringite phases. The AFm phases are layered double hydroxides. Its crystalline layer structure is derived from that of portlandite, but with one third of Al substitution by Ca. The resulting charge imbalance gives the layers a positive charge which is compensated by intercalated anions, e.g., SO42-, Cl-, OH-, etc. In the general formula, X represents one divalent or two monovalent interlayer anion. Generally, the inter-layer anions’ bonding are relatively weak, and this gives AFms remarkable ability to remove anionic contaminants. Two AFm phases were synthesized and they have different sizes and the same specific hexagon shape. The objective of this project is to evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-.
Batch experiment was conducted as a function of initial anionic concentration. Logarithms of removed molybdate amount and final aqueous anion concentration are plotted in Fig. 1. The data at low loading can be interpreted by Langmuir adsorption isotherms. And the dot lines of each sorption stage indicate the theoretical sorption capacities. When adding more Mo into the AFm system, the sorption process will go through anion exchange and Ca-precipitation meachnisms as the increasing coverage. From the aqueous results, AFm-Cl2 phase has a much stronger affinity and larger adsorption capacity for molybdate than AFm-SO4. For AFm-Cl2, above 95% molybdate was removed within 48 h, meantime, proportional inter-layer Cl- was released. The larger sorption capacity may result from the smaller size and more exchangeable intercalated anion.
The sorption products of reactor A-F were selected to be characterized by in-situ XRD and XAS.

## Slide 26
XAFS and in-situ time resolved XRD
Ma et al., ES&T, 2017
Notes: Generally, Portland cement is used to make the concrete cask and is composed of common phases, including gypsum, where C represents CaO, S SiO2, A Al2O3, and F is Fe2O3. Gypsum plays a very important role in controlling the hardening rate of the cement. Upon clinker cooling, a small amount of gypsum is introduced during the final grinding process, to slow down the “setting of cement”. On the other hand, each type of Portland cement contains C3A phases. Hydration of C3A is fastest and also generates most heat which will react with gypsum and mainly form AFm and ettringite phases. The AFm phases are layered double hydroxides. Its crystalline layer structure is derived from that of portlandite, but with one third of Al substitution by Ca. The resulting charge imbalance gives the layers a positive charge which is compensated by intercalated anions, e.g., SO42-, Cl-, OH-, etc. In the general formula, X represents one divalent or two monovalent interlayer anion. Generally, the inter-layer anions’ bonding are relatively weak, and this gives AFms remarkable ability to remove anionic contaminants. Two AFm phases were synthesized and they have different sizes and the same specific hexagon shape. The objective of this project is to evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-.
Batch experiment was conducted as a function of initial anionic concentration. Logarithms of removed molybdate amount and final aqueous anion concentration are plotted in Fig. 1. The data at low loading can be interpreted by Langmuir adsorption isotherms. And the dot lines of each sorption stage indicate the theoretical sorption capacities. When adding more Mo into the AFm system, the sorption process will go through anion exchange and Ca-precipitation meachnisms as the increasing coverage. From the aqueous results, AFm-Cl2 phase has a much stronger affinity and larger adsorption capacity for molybdate than AFm-SO4. For AFm-Cl2, above 95% molybdate was removed within 48 h, meantime, proportional inter-layer Cl- was released. The larger sorption capacity may result from the smaller size and more exchangeable intercalated anion.
The sorption products of reactor A-F were selected to be characterized by in-situ XRD and XAS.

## Slide 27
3. Anion exchange (D, E, F)
3. Anion exchange (D, E, F)
2. Edge sorption-Oh (B, C)
1. Edge sorption-Td (A)
2. Edge sorption-Oh (B, C)
1. Edge sorption-Td (A)
As the increasing coverage:
Ca atoms: green colour;
Al atoms: pink colour;
Mo atoms: cyan colour;
O atoms: red colour;
Cl atoms: light green colour;
H atoms: grey colour.

## Slide 28
Afm basal spacing vs. hydrated anion diameter
Ma et al., ES&T, 2017b
Notes: Generally, Portland cement is used to make the concrete cask and is composed of common phases, including gypsum, where C represents CaO, S SiO2, A Al2O3, and F is Fe2O3. Gypsum plays a very important role in controlling the hardening rate of the cement. Upon clinker cooling, a small amount of gypsum is introduced during the final grinding process, to slow down the “setting of cement”. On the other hand, each type of Portland cement contains C3A phases. Hydration of C3A is fastest and also generates most heat which will react with gypsum and mainly form AFm and ettringite phases. The AFm phases are layered double hydroxides. Its crystalline layer structure is derived from that of portlandite, but with one third of Al substitution by Ca. The resulting charge imbalance gives the layers a positive charge which is compensated by intercalated anions, e.g., SO42-, Cl-, OH-, etc. In the general formula, X represents one divalent or two monovalent interlayer anion. Generally, the inter-layer anions’ bonding are relatively weak, and this gives AFms remarkable ability to remove anionic contaminants. Two AFm phases were synthesized and they have different sizes and the same specific hexagon shape. The objective of this project is to evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-.
Batch experiment was conducted as a function of initial anionic concentration. Logarithms of removed molybdate amount and final aqueous anion concentration are plotted in Fig. 1. The data at low loading can be interpreted by Langmuir adsorption isotherms. And the dot lines of each sorption stage indicate the theoretical sorption capacities. When adding more Mo into the AFm system, the sorption process will go through anion exchange and Ca-precipitation meachnisms as the increasing coverage. From the aqueous results, AFm-Cl2 phase has a much stronger affinity and larger adsorption capacity for molybdate than AFm-SO4. For AFm-Cl2, above 95% molybdate was removed within 48 h, meantime, proportional inter-layer Cl- was released. The larger sorption capacity may result from the smaller size and more exchangeable intercalated anion.
The sorption products of reactor A-F were selected to be characterized by in-situ XRD and XAS.

## Slide 29
LDH sorption of redox-sensitive anions: conclusions
Notes: Generally, Portland cement is used to make the concrete cask and is composed of common phases, including gypsum, where C represents CaO, S SiO2, A Al2O3, and F is Fe2O3. Gypsum plays a very important role in controlling the hardening rate of the cement. Upon clinker cooling, a small amount of gypsum is introduced during the final grinding process, to slow down the “setting of cement”. On the other hand, each type of Portland cement contains C3A phases. Hydration of C3A is fastest and also generates most heat which will react with gypsum and mainly form AFm and ettringite phases. The AFm phases are layered double hydroxides. Its crystalline layer structure is derived from that of portlandite, but with one third of Al substitution by Ca. The resulting charge imbalance gives the layers a positive charge which is compensated by intercalated anions, e.g., SO42-, Cl-, OH-, etc. In the general formula, X represents one divalent or two monovalent interlayer anion. Generally, the inter-layer anions’ bonding are relatively weak, and this gives AFms remarkable ability to remove anionic contaminants. Two AFm phases were synthesized and they have different sizes and the same specific hexagon shape. The objective of this project is to evaluate the capacity of AFm-SO4 and AFm-Cl2 to retard the mobility of SeO32- and MoO42-.
Batch experiment was conducted as a function of initial anionic concentration. Logarithms of removed molybdate amount and final aqueous anion concentration are plotted in Fig. 1. The data at low loading can be interpreted by Langmuir adsorption isotherms. And the dot lines of each sorption stage indicate the theoretical sorption capacities. When adding more Mo into the AFm system, the sorption process will go through anion exchange and Ca-precipitation meachnisms as the increasing coverage. From the aqueous results, AFm-Cl2 phase has a much stronger affinity and larger adsorption capacity for molybdate than AFm-SO4. For AFm-Cl2, above 95% molybdate was removed within 48 h, meantime, proportional inter-layer Cl- was released. The larger sorption capacity may result from the smaller size and more exchangeable intercalated anion.
The sorption products of reactor A-F were selected to be characterized by in-situ XRD and XAS.

## Slide 30
To students:
- Bin Ma Caroline
Bissardon
To former postdocs:
- Mingliang Kang, Fabrizio Bardelli, Sudipto Chakraborty..
To colleagues:
- Alejandro Fernandez Martinez,
Kideok Kwon, Andreas Scheinost..
To funding agencies:
Acknowledments

## Slide 31
Take home message
Mineral surfaces (calcite, Fe oxyhydroxides..) are active sorbant for 14C carbonateand 79Se Selenite via adsorption and co-recipitation reactions, leading to Kd >>0
Multiple barriers: canister corrosion layer and concrete, present redox active actors RN sorption capacities (e.g. on AFm DHLs structures, but NOT via anion exchange)
Contaminant aqueous + solid speciation: EXAFS + XANES + XPS + wet chemistry; EXAFS, with increasing competition with HE-XRD and PDF analysis + molecular computation (ab initio DFT, MD..)
In situ Eh pH for complex systems such as concrete can be measured based on mixed spectroscopic and chemical measurements
… and welcome to Grenoble!