## Slide 1: CArbon-14 Source Term CAST
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Name: Michel Herm
Organisation: KIT-INE
Date: 16.01.2018

## Slide 2: Introduction
Determination of 14C inventory in Zircaloy-4 of an irradiated PWR fuel rod segment and chemical form of 14C released from the material.
Comparison of experimentally obtained radionuclide inventories with theoretically predicted inventories.

## Slide 3: Materials & irradiation characteristics
Zircaloy-4 cladding sampled from the plenum of fuel rod segment SBS1108–N0204.
Irradiated in the Swiss Gösgen PWR (1985 to 1989).
1226 effective full power days.
Average burn-up: 50.4 GWd/tHM.
Average linear power: 260 W/cm.
length of segment: 500 mm
dose rate ~20 mSv/h
dose rate ~1600 mSv/h
stainless steel
Zircaloy-4

## Slide 4: Preparation of subsamples
dissolution experiments in glove box
dose rate ≤ 0.3 mSv/h
Preparation of small subsamples by dry cutting in a shielded box.
subsample # | 1 | 2 | 3 | 4 | 5 | 6
mass [g] | 0.184 | 0.130 | 0.120 | 0.178 | 0.189 | 0.183
dose rate [mSv/h] | ≤ 0.27 | ≤ 0.15 | ≤ 0.17 | ≤ 0.26 | ≤ 0.28 | ≤ 0.22
Zircaloy-4:

## Slide 5: Dissolution experiments
Dissolution of Zircaloy-4 subsamples in glove box using a flask or autoclave.
aqueous samples
gaseous samples
14C extraction system
gas-MS
dissolution experiments
Autoclave experiments performed under anoxic conditions (Ar atmosphere).

## Slide 6: 14C extraction set-up and procedure
absorption of 14CO2/CO2 in various washing bottles
determination of [14C] by LSC
acid digestion in autoclave
acid digestion in glass reactor
dissolved hydrocarbons
acidic digestion liquor
wet oxidation
(K2S2O8, AgNO3, 95°C)
catalytic furnace
(CuO, Pt/Al, 750°C)
gases released during digestion / gaseous samples
CO, gaseous hydrocarbons
CO2
gas-MS
1
2
3
4
5
6
7
8

## Slide 7: Inventory calculations
Calculation of the radionuclide inventory of the irradiated plenum Zircaloy-4 cladding.
MCNP code to simulate neutron flux, and CINDER module for bur-up and activation calculation.
SCALE/TRITON package to simulate neutron flux, and ORIGEN-S program for burn-up and activation calculation.
Geometrical shape, nominal material composition, irradiation characteristics, and position in fuel assembly and nuclear reactor taken into account.

## Slide 8: Inventory calculations
Burn-up conditions of the fuel rods adapted in such a way that the given boundary conditions of 50.4 GWd/tHM and irradiation time of 1226 days by ~260 W/cm will be kept.
green fuel pins: investigated fuel segments (symmetry, statistic error)
guide tubes: filled with water (control rods extracted)
yellow fuel pins: generating power and thus flux without burn-up
dark blue: water of primary circuit

## Slide 9: Inventory calculations
Calculation of plenum Zircaloy-4 cladding radionuclide inventory based on:
  Minor actinides/fission products: U traces in Zircaloy (max 3.5 ppm).
  Activation products: precursor elements present in Zircaloy (e.g. 14N, 54Fe, 124Sn).
N content in Zircaloy and use in activation calculations:
Nominal composition data for Zircaloy-2 and Zircaloy-4: < 80 ppm N.
Gras 2014 / Sakuragi et al. 2013 recommend 40 ppm N for Zircaloy-2 and Zircaloy-4.
Marimbeau 2004 recommend 34 ± 10 ppm N for Zircaloy-4.
N content in non-irradiated Zircaloy-4 investigated by KIT is about 30 ppm.
Uncertainty of N content in Zircaloy in general smaller compared to stainless steels.

## Slide 10: Results
14C inventory in irradiated Zircaloy-4: 3.7(±0.4)×104 Bq/g.
Experimental and calculated results in good agreement for 14C, 55Fe, 125Sb.
Experimental activities agree, within analytical uncertainty, with calculations.
 | 14C | 55Fe, 125Sb | 
 | digestion liquor + gas phase | digestion liquor | 
Separation technique | 14C extraction system | extraction column | –
Method | LSC | LSC | -spectroscopy
Calculated 14C inventory (30 ppm N):
MCNP/CINDER: 3.5×104 Bq/g
SCALE/TRITON/ORIGEN-S: 3.6×104 Bq/g

## Slide 11: Summary and conclusions
Zircaloy-4 cladding specimens digested in dilute acid and content of 14C released into aqueous and gaseous phase successfully analysed.
Experimentally determined inventories are in good agreement with calculated.
Uncertainty of N content in Zircaloy in general smaller compared to stainless steels.
Local neutron flux around sample in reactor and N content in steel are key parameters for accurate 14C inventory calculations.

## Slide 12: Acknowledgments
Funding:
Thank you for your attention!
The research leading to these results has received funding from the European Union’s European Atomic Energy Community’s (Euratom) Seventh Framework Programme FP7/2007-2013 under grant agreement no. 604779, the CAST project.
M. Böttle | V. Metz
E. Bohnert | N. Müller
R. Dagan (INR) | INE workshop
E. González-Robles | INE infrastructure team
B. Kienzler | 
P. D. W. Bottomley | R. Nasyrow
R. Gretter | D. H. Wegen
S. Caruso |