## Slide 1: CArbon-14 Source Term CAST
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Name: Suzuki-Muresan T.
Organisation: SUBATECH/ARMINES
Date: 16/01/2018

## Slide 2: Analytical strategy to measure 14C released from irradiated zircaloy
T. Suzuki-Muresan, M. A. Bahri, R. Bouakkaz, M. B. Mokili, C. Landesman, A. Abdelouas
V. Broudic, S. Perrin
S. Necib

## Slide 3: Context: Irradiated nuclear materials
Pictures modified from IRSN source and « Les combustibles nucléaires - Le combustible des réacteurs à eau » (CEA)
Ewing (2015) Long-term storage of spent nuclear fuel, Nature

## Slide 4: Origin of carbon-14 in zircaloy claddings
Formation via neutron activation
  From impurity in zircaloy cladding : 14N (n, p) 14C
  From zirconium oxide layer formed at surface : 17O (n, α) 14C
Ewing (2015) Long-term storage of spent nuclear fuel, Nature / Ewing and Bruno, Elements, 2 (2006) 343 / Photo from CEA
 Complex chemical composition
Neutron activation
Spent fuel
Zircaloy (Zr)
ZrO2

## Slide 5: Fate of fuel rods in nuclear fuel cycle
Christian BARANDAS / AREVA, COGEMA/DR, Les combustibles nucléaires - Le combustible des réacteurs à eau » (CEA)
http://www.laradioactivite.com/fr/site/pages/OperationRetraitement.htm, POSIVA, Pictures from AREVA
Separation of metallic structures and nuclear spent fuel during reprocessing
Hulls
End-fittings
Compaction
Waste
conditioning
Repository in deep
geological formation
 Compaction of metallic structures in cementitious media
Clayey host rock
Eng. Barr. Syst.
Cement

## Slide 6: Issues for long-term repository
Clayey host rock
Eng. Barr. Syst.
Importance of 14Corganic in the radioactive waste inventory
  Contribution to the total dose
Focus on the characterization of 14Corganic fraction released in the leaching solution
  particularly analysis of ion carboxylic acids having a short carbon chain ≤ 5.
14C
14Corganic
14Cinorganic
SPECIATION ?
?
Cement
14C
DIFFUSION ?
 Determination of 14Corganic speciation in alkaline aqueous media (pH ~12)

## Slide 7: Methodology

## Slide 8: In repository conditions
Clayey host rock
Eng. Barr. Syst.
14C
14Corg
14Cinorg
speciation
Cement
14C activities expected to be extremely low
highly diluted compared to the other radionuclides
137Cs
90Sr
106Ru/106Rh
125Sb
actinides
 | 6 months | 3 years
C-14 (Bq*) | 0,1 | 10
Cs-137 (Bq*) | 150 | 500
Scaling ratio C-14 vs Cs-137
* Activity after 6 months corrected to the value at the start of the immersion test, V =20mL (Tanabe and al.)
T. Yamaguchi and al. A study on chemical forms and migration behavior of radionuclides in hull waste, 1999
European Commission Final Report (EUR 19132 EN), Spent Fuel Disposal Performance Assessment (SPA project), Nuclear Science and Technology, 2000

## Slide 9: Analytical strategy
Extreme low 14C activity released in solution
  Separation from other RNs
Non neglectible contributions of beta emitters (137Cs and 125Sb)
Eliminate a maximum of radionuclides
  Preservation of 14C speciation
Need to develop analytical strategy
  Decontamination
  Separation, analyses, measurements
Decontamination ( details in Poster)
  K2[CuFe(CN)6] without organic binding
  High selectivity and high exchange capacity
  Extraction of major RNs
  Radiation resistance
Leaching solution NaOH, pH 12
(14C, 60Co, 137Cs, 125Sb, …)
Decontamination leaching solution
Liquid Scintillation Counting
Accelerator Mass Spectrometry
Ion Chromatography

## Slide 10: Leaching experiment performed at CEA
Hulls reference | M5 | MOX D4
Cladding material | M5 | Inner layer = Zy-4 Outer layer= Zr-0.8%Sn
Fuel type | UOx (3.88% 235U) | MOX (7.2% Pu)
Number of cycles | 3 | 4
Irradiation time | 1937 days | 2293 days
Mean Burn up | 46,570 MWd/tHM | 54,500 MWd/tHM
Reactor (PWR) | EDF Nogent 2 (France) | Gösgen (Switzerland)
Discharged from reactor | June 2004 | June 2002
Output of AREVA | October 2009 | Sept. 2008
Activity (GBq) | 0.81 | 3.57
Characteristics of hulls | ~35 mm length diameter = 9.5mm / thickness = 0.57mm | 
Mass | ~ 3.5 – 5.5 g / hull | 

## Slide 11: Leaching experiment performed at CEA
Hot cells (RT 25°C)
Glove box lab
Leaching experiments
Radiochemical analysis
Internal sample
transfer
CEA Marcoule
External
transfer
LASE
LRMO
SUBATECH
IMT
Atlantique
CEA Saclay
αβγ activities
14C analyses
Ensure the acceptability of the samples
M5 hulls  02/02/2016
D4 hulls  20/09/2016
+6m
+6m
+2w
+2w

## Slide 12: Leaching experiment performed at CEA
Static leaching solution
  Alkaline NaOH solution, pH12
  De-aerated water by bubbling with Ar
  No solution renewal
  Anoxic conditions : Ar-gas glove box
2 hulls / reactor
Ar gas inlet
Gas purge
Solution sample
Lid
Ar atm.
Ti liner
Leaching solution
Hulls
SS / Ti cylinder

## Slide 13: Analytical methods
Ion chromatography
  Ion column exclusion
    Formate, acetate, propionate
  Anion column
    Oxalate
Liquid scintillation counting
  Detection limit 0.02 Bq/mL
AMS
  @ VERA: Vienna Environmental Research Accelerator
  14C organic fractions
 | Anion. Col. | ICE
Device | IC Compact 881 Metrohm | IC Compact 881 Metrohm
Column | Metrosep Asupp 16 250-2.0 | IonPac ICE-AS6 Exclusion Column
Detection | Conductivity | Conductivity
pH solution | Adjusted at 8 | Adjusted at 8
Eluant | Na2CO3 : 7.5 mM NaOH : 0.75mM | 0.1 mM TFA
Pump flow | 0.15 mL/min | 1 mL/min
Injection volume | 250 µL | 250 µL

## Slide 14: AMS
AMS counts individual atoms in a sample rather than radioactive decay events (=LSC)
  the most sensitive analytical technique
AMS measures radioisotopes through isotope ratios
  Typical radioisotope/stable isotope ratios = 10−12 to 10−16
  In CAST project, total ratio 14C/12C = ~10-6
    6 orders of magnitude higher than the acceptable ratio
    Typical measurement 14C/12C not performed:
      to prevent underestimation of 14C
    Ratio 14C/13C measured: addition of an isotopic pure carbon 13: glucose
Sample treatment
  Oxidation of organic carbon by UV light inside closed quartz vials.
  Oxidation process formed CO2(g) and the fraction released in the head volume was extracted for AMS measurements.
  The chemical yield of this method is 50-70%.

## Slide 15: Speciation of 14C in alkaline aqueous media

## Slide 16: Leaching solution
Leaching solution NaOH, pH 12
(14C, 60Co, 137Cs, 125Sb, …)
Decontamination leaching solution
K2[CuFe(CN)6]
M5-14days
M5-6months
D4-14days
D4-6months
Efficient decontamination
Confirmed with αTβT counting
Liquid Scintillation Counting
Accelerator Mass Spectrometry
Ion Chromatography

## Slide 17: Leaching solution
Leaching solution NaOH, pH 12
(14C, 60Co, 137Cs, 125Sb, …)
Decontamination leaching solution
K2[CuFe(CN)6]
Liquid Scintillation Counting
Accelerator Mass Spectrometry
Ion Chromatography
Formate
Acetate
Propionate
Formate/Acetate
Propionate
Nitrate
Oxalate
Butyrate
Chloride
Exclusion column
Anion column
Collection of fractions yield between 25-85%

## Slide 18: Quantification / Speciation of carboxylic acids
TIC = 93%TC
M5-hulls
Formate 1.0%TC
Acetate 1.1%TC
Propionate 1.6%TC
Oxalate 2.5%TC
not identified 1.3%TC
TIC = 96%TC
Zy4-hulls
14C-carboxilic acid 0.002%TOC
0.0002%TC
Formate 0.5%TC
Acetate 0.4%TC
Propionate <LD
Oxalate 0.1%TC
not identified 2.7%TC
14C-carboxilic acid 0.004%TOC
0.0002%TC
Inorganic carbon dominates the contribution of TC inventory: TOC ~4-7%TC
carboxylic acid 27%TOC
carboxylic acid 83%TOC
Low contribution of 14C-carboxylic acid regarding the TC inventory
Successful collection of carboxylic organic fractions

## Slide 19: Quantification / Speciation of carboxylic acids
carboxylic acids | LSC 14C zircaloy-4 / 14 days |  | LSC 14C zircaloy-4 / 6 months | 
Formate | 370 Bq/g hulls | 23×10-10 g/g hulls | 365 Bq/g hulls | 22×10-10 g/g hulls
Acetate | 249 Bq/g hulls | 15×10-10 g/g hulls | 327 Bq/g hulls | 20×10-10 g/g hulls
Propionate | 119 Bq/g hulls | 7×10-10 g/g hulls | 36 Bq/g hulls | 2×10-10 g/g hulls
Oxalate | 14 Bq/g hulls | 0.9×10-10 g/g hulls | 36 Bq/g hulls | 2×10-10 g/g hulls
carboxylic acids | LSC 14C M5® / 6 months | 
Formate | 179 Bq/g hulls | 11×10-10 g/g hulls
Acetate | 71 Bq/g hulls | 4×10-10 g/g hulls
Propionate | 65 Bq/g hulls | 4×10-10 g/g hulls
Oxalate | 19 Bq/g hulls | 1×10-10 g/g hulls
14C Zy4 : ~800 Bq/g hulls
14C M5 : ~330 Bq/g hulls
Influence of ZrO2 layer?
Activities close to DL
High uncertainties : ~50-100%

## Slide 20: Quantification / Speciation of carboxylic acids
LSC (uncertainties 50-100%)
14 days: ~800 Bq/g hulls
6 months: ~760 Bq/g hulls
AMS (uncertainties 25%)
14 days : ~1.5 Bq/g hulls
6 months : ~3 Bq/g hulls
High 14C activities by LSC compared with AMS
Confirmation of 14C organic fraction by AMS: carboxylic acids
Need of complementary analyses to correct LSC/AMS data
carboxylic acids | 14C zircaloy-4 / 14 days |  | 14C zircaloy-4 / 6 months | 
 | LSC | AMS | LSC | AMS
Formate | 370 Bq/g hulls | 0.1 Bq/g hulls | 365 Bq/g hulls | 0.06 Bq/g hulls
Acetate | 249 Bq/g hulls | 0.6 Bq/g hulls | 327 Bq/g hulls | 0.09 Bq/g hulls
Propionate | 119 Bq/g hulls | 0.3 Bq/g hulls | 36 Bq/g hulls | 0.07 Bq/g hulls
Oxalate | 14 Bq/g hulls | 0.3 Bq/g hulls | 36 Bq/g hulls | pending

## Slide 21: Quantification / Speciation of carboxylic acids
carboxylic acids | 14C zircaloy-4 / 14 days |  | 14C zircaloy-4 / 6 months | 
 | LSC | AMS | LSC | AMS
Formate | 370 Bq/g hulls | 0.1 Bq/g hulls | 365 Bq/g hulls | 0.06 Bq/g hulls
Acetate | 249 Bq/g hulls | 0.6 Bq/g hulls | 327 Bq/g hulls | 0.09 Bq/g hulls
Propionate | 119 Bq/g hulls | 0.3 Bq/g hulls | 36 Bq/g hulls | 0.07 Bq/g hulls
Oxalate | 14 Bq/g hulls | 0.3 Bq/g hulls | 36 Bq/g hulls | pending
carboxylic acids | LSC 14C M5® / 6 months | 
 | LSC | AMS
Formate | 179 Bq/g hulls | 0.5 Bq/g hulls
Acetate | 71 Bq/g hulls | 0.1 Bq/g hulls
Propionate | 65 Bq/g hulls | 0.1 Bq/g hulls
Oxalate | 19 Bq/g hulls | 8.5 Bq/g hulls
Difficulty to give a clear tendency
In all samples: presence of carbon-14 carboxylic acids

## Slide 22: Conclusion on the analytical strategy
Leaching solution NaOH, pH 12
(14C, 60Co, 137Cs, 125Sb, …)
Decontamination leaching solution K2[CuFe(CN)6]
Liquid Scintillation Counting
Accelerator Mass Spectrometry
Ion Chromatography
TIC/TOC
αTβT
γ
Ion Exclusion Column
Anion column
Small carboxylic acid fractions collected: formate, acetate, propionate, oxalate
Confirmation of 14C labeled molecules
Correction between LSC - AMS data

## Slide 23: Conclusion & Perspective
 | Zy4-type hulls | M5-type hulls
Mean Burn up | 54,500 MWd/tHM | 46,570 MWd/tHM
14C act. metal. (Calculation) | ~17,800 Bq/g | ~30,300 Bq/g
14C act. leach. (CAST) | 800 Bq/g | 330 Bq/g
14C leach/14C metal | ~4-5 % | ~1%
Gras [2014]. State of the art of 14C in zircaloy and Zr alloys - 14C release from zirconium alloy hulls. CAST Project Report.
Caron et al. [2017] Final report on C-15 released from irradiated zircaloys in NaOH Solution: quantification and speciation of C-14, D3.18. CAST Project Report.
Small amount of 14Corg released in aqueous media in repository conditions
14 days and 6 months leaching at 25°C: need of long term experiments and higher T°C to confirm the results, micro-characterisation of solid (ZrO2 layer)

## Slide 24: Acknowledgments
Christophe Jégou
I. Deniau, G. Guerel, E. Fisson,
A. Drouain, C. Mérignac, V. Baty, A. Piscitelli
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
J. Molina, F. Cochin
Peter Steier
Steve Williams and Simon Norris
Jens Mibus (WP2-lead)
and Sophia Necib (WP3 lead)
All WP2 and WP3 partners
Reviewers and EUG members