## Slide 1: Zircaloy-4 corrosion in high pH solutions: Study of the carbon-based molecule production
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Sébastien Caes, Frank Druyts
SCK•CEN
scaes@sckcen.be
16/01/2018

## Slide 2: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 3: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 4: Context
This research is part of the International CAST (CArbon-14 Source Term) project. Its goals are:
  To improve understanding of the C and 14C release during corrosion of radioactive waste materials under disposal repository conditions
  To have a corrosion rate estimation and carbon-released speciation

## Slide 5: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 6: Accelerated Corrosion
Experimental vial

## Slide 7: Static Corrosion
Experimental vial

## Slide 8: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 9: Samples
Non-irradiated Zircaloy-4
wt.% |  |  |  | µg/g |  |  |  |  | 
Sn | Cr | Fe | Zr | C | Hf | Si | W | O | N
1.2-1.7 | 0.07-0.13 | 0.17-0.24 | Bal. | 270 | 100 | 120 | 100 | 1000-1400 | 25
Unirradiated Zircaloy-4 specimen
Unirradiated Zircaloy-4 Composition

## Slide 10: Samples
TEM structure analysis of unirradiated Zircaloy-4
  The structure shows small uniform equiaxed grains (Figure A). Black spots are attributed to Laves phases (Figure A and C)
  Laves phase composition is Zr(Fe,Cr)2
  Dislocation lines defects with a density of 4.1×1013/m² (Figure B)
  Presence of elongated ZrC precipitates (Figure D)
(A)
(A)
(A)
(B)
(A)
(C)
(A)
(D)

## Slide 11: Samples
Irradiated Zircaloy-4
Sample before cutting
Dose rates of Zircaloy-4 samples
Sample after cutting (samples A,B and C for leaching tests ; E for polarised tests)
Sample code
Dose rate (through a plastic vial)
(µSv/h)
FF6678-R4-A
FF6678-R4-B
FF6678-R4-C
450 (09/09/2016)
270 (09/09/2016)
200 (09/09/2016)
FF6678-R4-E
113 (15/02/2017)
~20.5 mm
9.7 mm

## Slide 12: Samples
Irradiated Zircaloy-4
Results from g-ray spectrometry of sample E
Nuclides | Activity (Bq) | Uncertainties (Bq) | t1/2 (years)
Mn-54 Co-60 Cs-137 Zr-95 Ru-106 Sn-113 Sb-125 Cs-134 Ce-144 Nb-95 | 1.68E+03 2.78E+04 1.24E+03 1.98E+04 1.33E+03 7.7E+03 1.43E+05 255 1.88E+03 4.40E+04 | 0.34E+03 0.56E+04 0.25E+03 0.40E+04 0.40E+03 1.5E+03 0.29E+05 89 0.38E+03 0.88E+04 | 0.85 5.27 30.19 0.18 1.02 0.32 2.76 2.07 0.78 0.10

## Slide 13: Samples
TEM structure analysis of irradiated Zircaloy-4 (Cladding)
  The grain structure shows a narrow lath structure due to the rolling process to produce the cladding (Figure A)
  Dislocation lines density is comparable with unirradiated Zircaloy-4 (Figure B)
  Presence of small dislocation loops (Figure C and D)
(A)
(B)
(C)
(D)

## Slide 14: Samples
TEM structure analysis of irradiated Zircaloy-4 (end-plug)
  The grain structure shows equi-axed grains (Figure A)
  Observation of fringe-like defect contrast (Conduroy Contrast ; Figure B)
  Laves phase precipitates are still present (Figure C)
  Light amorphisation due to neutron irradiation
(A)
(B)
(C)

## Slide 15: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 16: Gas Chromatograph
Shin Carbon ST column
  Ideal for permanent gas/light hydrocarbon separation
Pulse Discharged Helium Ionization Detector (PDHID)
  Detection limit of 50 ng/g (50 ppb)
ShinCarbon ST column in the GC oven
Scheme of a PDHID detector

## Slide 17: Gas Chromatograph
Calibration
Chromatogram of a mixture of different gas at a 10 µg/g concentration
Retention time (minutes)
Intensity (a.u.)

## Slide 18: Gas Chromatograph
Calibration
  Presence of unexpected peaks in the chromatograms

## Slide 19: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 20: Accelerated tests
Sample preparation
Glueing
Embedding
Polishing

## Slide 21: Accelerated tests
Polarisation curves – Zry-4 – Ca(OH)2
Chart: 
Unirradiated
Irradiated
Potential (V vs. Ag/AgCl)
Current (A)
-0.75 V

## Slide 22: Accelerated tests
Corrosion rate estimation from I vs. t curves
  Unirradiated Zircaloy-4 – Ca(OH)2
Chart: 
Current (|A|)
Corrosion time (h)
V = -0.75 V vs. Ag/AgCl

## Slide 23: Accelerated tests
Corrosion rate estimation from I vs. t curves
Mean produced current (<I>) = 5.4 x10-9 A
Total charge = <I> x t = 5.9 x10-9 x 604510 = 3.27 x10-3 C
If only the oxidisation of Zr° in Zr4+ is considered:
3.27 x10-3 C corresponds to 8.5 x10-9 mol of Zr corroded
= 7.7 x10-7 g of Zircaloy-4 (Zirconium)
Depth of corrosion = 0.88 nm (after 7 days)
Corrosion rate = 54 nm/year (4 nm/year for irradiated sample)

## Slide 24: Accelerated tests
Chart: 
Irradiated
Unirradiated
CO2
Ghost peaks
H2
GC – Zry-4 – Ca(OH)2
  Corrosion time: 7 days
Retention time (minutes)
Intensity (a.u.)
  No detectable carbon-based gas formation
  Addition of chloride to increase the corrosion rate

## Slide 25: Accelerated tests
Polarisation curves – Zry-4 – Ca(OH)2 + CaCl2
Potential (V vs. Ag/AgCl)
Current (A)
Chart: 
Unirradiated
Irradiated
0.62 V
1.00 V

## Slide 26: Accelerated tests
GC – Zry-4 – Ca(OH)2 + CaCl2
  Corrosion time: ~5 hours
   Big peak due to the production of methane
CH4
H2
CO2
Chart: Retention time (minutes)
Irradiated
Unirradiated

## Slide 27: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 28: Static Tests
GC – Zircaloy-4 (195 leaching days)
Chart: Retention time (minutes)
Zr-A
Zr-B
Zr-C
CO2
CH4
H2
C2H4

## Slide 29: Static Tests
GC – Zircaloy-4 (195 leaching days)
Sample | Methane |  | Ethene |  | Carbon dioxide | 
 | Measured peak area | Calculated concentration (µL/L) | Measured peak area | Calculated concentration (µL/L) | Measured peak area | Calculated concentration (µL/L)
Zr-A | 445448 | 6.4 ± 0.3 | 87015 | 1.0 ± 0.1 | 461671 | 5.0 ± 2.0
Zr-B | 481731 | 7.0 ± 0.4 | 104984 | 1.2 ± 0.1 | 341713 | 3.2 ± 2.0
Zr-C | 410637 | 5.9 ± 0.3 | 72075 | 0.8 ± 0.1 | 364723 | 3.6 ± 2.0
Mean value | - | 6.4 | - | 1.0 | - | 3.9

## Slide 30: Static Tests
GC – Zry-4: Corrosion rate approximation
Hypotheses: - Homogeneous corrosion process
- Carbon homogeneously present in Zircaloy-4
- All released carbon is transformed in methane, ethene or CO2
Calculation:
Gas volume (L) = headspace volume (L) x gas concentration (µL/L)
 Gas weight (g) = gas volume (L) x gas density (g/L)
Number of moles of gas (mol) = gas weight (g) / gas molecular weight (g/mol)

## Slide 31: Static Tests
GC – Zry-4: Corrosion rate approximation
Calculation:
Number of moles of CH4 = 3.96 x10-9 mol = Number of moles of C
Number of moles of C2H4 = 1.22 x10-9 mol = ½ Number of moles of C
Number of moles of CO2 = 2.51 x10-9 mol = ½ Number of moles of C
Moles of carbon released = 3.96 x10-9 + 2x 1.22 x10-9 + 2x 2.51 x10-9
= 1.14 x 10-8 mole

## Slide 32: Static Tests
GC – Zry-4: Corrosion rate approximation
Calculation:
Weight of released carbon = Moles of released carbon x molecular weight of carbon
Weight of corroded Zircaloy-4 = weight of released carbon / concentration of carbon in the Zircaloy-4
 Corrosion depth = (weight of corroded Zircaloy-4 / density of Zircaloy-4) / surface area
Depth of corrosion of C-Steel: 45 nm after 195 days
Mean corrosion rate of Zircaloy-4: 84 nm/year
Mean corrosion rate of Zircaloy-4 (without CO2): 57 nm/year

## Slide 33: Outline
Context
Corrosion tests
Zircaloy-4 samples
Gas analysis by gas chromatography
Accelerated corrosion tests
  Polarisation curves
  Carbon speciation in the gas phase
Static corrosion tests
Conclusions

## Slide 34: Conclusions
Two kind of corrosion tests: accelerated and static tests
Accelerated corrosion tests
  Polarisation curves showed some electrochemical differences due to irradiation
  No differences due to irradiation on the carbon speciation
  Detection of methane in the gas phase in presence of chlorides
  I vs. t curves of the unirradiated Zircaloy-4 gave an approximate corrosion rate of 54 nm/year
Static corrosion tests
  Detection of methane, ethene and possibly CO2 by GC
  Based on gas production concentration, a corrosion rate of 57 to 84 nm/year was approximated

## Slide 35: Acknowledgments
Technical assistance
  Pieter Schroeders
  Sabrina Lunardi
  Wim Verwimp
  Ben Gielen
  Steven Smets
  Wouter Van Renterghem
The authors gratefully acknowledge the financial support of this work by ONDRAF/NIRAS, the Belgian national radioactive waste management organisation
And the audience for listening…