## Slide 1: CArbon-14 Source Term CAST
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Name: Sophia Necib
Organisation: Andra
Date: 16/01/2018

## Slide 2: WP3 session
Introduction
Oral communications (4 CAST invited speakers + 1 external invited speaker):
  C-14 inventory in irradiated Zr (M.HERM – KIT)
  Leaching tests and corrosion measurements for irradiated Zr (C. BUCUR – RATEN ICN)
  Analytical strategy to measure C-14 released from irradiated Zr (T.SUZUKI - SUBATECH)
  Corrosion rate measurements on Zr-4 in alkaline media (S.CAES - SCK.CEN)
  Corrosion of Zirconium alloys and C-14 release from compacted waste (A.AMBARD – EDF)
  WP3 Summary and conclusions (S.NECIB – Andra)
Poster presentations
  Analytical strategy for measurement of C-14 in leachate of irradiated zirconium alloy hulls (L.KASPRZAK et al. - CEA)
  Analytical strategy for the measurement of C-14 in alkaline solution (T.SUZUKI et al. – SUBATECH)
  Corrosion behaviour of irradiated and non-irradiated zirconium alloys: investigations on corrosion rate, released C-14 species and IRF (T.SAKURAGI – RWMC)
  C-14 determination in irradiated steel and Zircaloy: Progress at JRC Karlsruhe in the realm of the CAST Project (D.Bottomley et al.- JRC – ITU)

## Slide 3: Objectives WP3 “Zircaloy”
To obtain a better understanding of 14C behaviour in zirconium alloy fuel claddings under disposal conditions with regard to:
  Inventory
    Origin, location and distribution of 14C and its precursors (N, C, O) in zirconium alloys and in outer oxide layer,
    Influence of several parameters: burnup, BWR/PWR, zirconium alloys
    Comparison between modelling and experiments
  Release mechanisms from waste packages
    Corrosion of irradiated zirconium alloys
    Corrosion of unirradiated zirconium (for comparison)
    Solubility of zirconium oxide and 14C migration in zirconium oxide
  Speciation
    Organic / inorganic species
    Identification of organic compounds

## Slide 4
WP3 “Zircaloy”Description
WP3
Task 3.4
Task 3.1
Task 3.2
Task 3.3
State of the Art
D3.1
Analytical development
D3.3
D3.7
D3.9
Leaching experiment
+
C-14 measurements (inventory, speciation, quantification)
Corrosion rate measurements
D3.2
D3.4-D3.8
D3.10-D3.19
MS5
Final synthesis
D3.20
MS9

## Slide 5: WP3 - Partners
RWMC
WP3
RATEN ICN
CEA
SUBATECH
KIT
SCK.CEN
AREVA
ANDRA
JRC
EDF

## Slide 6
What did we know before CAST?

## Slide 7
Task 3.1
D3.1 : “State of the art of 14C in Zircaloy and Zr alloys - 14C release from Zr alloy hulls” (J.M Gras)
History of Zr alloys claddings in reactor
Origin and inventory of 14C
Release mechanisms of 14C
Corrosion of Zircaloys
Speciation of released 14C

## Slide 8: Task 3.1: History of Zr alloys
Zr alloys :
  in PWR : Zr-4, M5TM (Zr-1Nb), ZirloTM (Zr-1Sn-1Nb)
  in BWR : Zr-2
N, impurity element, very predominant precursor of 14C (14N(n,p)14C)
Specified values N < 80ppm
Notes: Zy 4 equivalent to Zy 2 with non Ni to reduce H uptake during oxidation in primary circuit

## Slide 9
External oxide layer (cont.)
  Its thickness depends on the Zr alloy
  The Oxide thickness increases with the BU
Bossis et al., 2006
Experience in PWR : Zy-4 > ZirloTM > Optimized ZirloTM > M5TM
Hulls from new Zr alloys will be less oxidised
Task 3.1: History of Zr alloys

## Slide 10
Before CAST:
    Many data available from calculations
    Calculations (with  40 or 80 ppm N)
    PWR (Zy-4, M5TM) and BWR (Zy-2)
    Metal and oxide:
      14C in oxide > 14C in metal
      RWMC results
Chart: Burn-up (GWd.t-1)
| 22.4 | 27.49 | 27.5 | 28 | 39.4 | 29.5 | 31 | 31.1 | 31.5 | 32 | 32.9 | 33 | 33.1 | 35.700000000000003 | 39.5 | 39.700000000000003 | 40 | 41 | 43 | 43.1 | 45 | 47.9 | 48.9 | 48.95 | 49 | 50 | 51 | 70
BWR - RWMC | 19 | 23.3 | 26.9 | 28 | 17.4 | 30
BWR - other | 23 | 52 | 15
PWR - RWMC | 27.7 | 27.7 | 27.9 | 28.5 | 30.8 | 31.4 | 33.1 | 33.4 | 30 | 40 | 33.3 | 33.4 | 34.1 | 34.5
PWR - CEA, EDF | 33 | 48.33
PWR - other | 17 | 15 | 24 | 33 | 17
in kBq/g Zr | Metal | Oxide
PWR (47.9 GWd/t) | 30 | 59
BWR (39.4 GWd/t) | 19 | 44
Task 3.1: Origin and Inventory of 14C in claddings

## Slide 11
Task 3.1: Release mechanisms
of 14C
Two systems
  the oxides formed in reactor :
    internal layer ( 10 µm)
    external layer ( 100 µm)
  the metal
Three main processes
  oxides :
    dissolution (chemical process : pH, complexing species…)
    diffusion or other mechanism of migration of 14C
  metal : uniform (general) corrosion (electrochemical process, stability of oxide film)
Environment (deaerated conditions)
  cementitious water
  « neutral » (argillaceous) water
C-14 release in aqueous solution

## Slide 12: Task 3.1:Corrosion of Zircaloy in alkaline water at low Temperature
12
Chart: Test duration (day)
| 30 | 30.1 | 90 | 90.1 | 180 | 180.2 | 365 | 365.1 | 730 | 730.1 | 1825 | 1825.1
Zy4 - 30°C | 4.1918 | 5.9178 | 5.4247 | 6.7 | 5.7 | 7 | 7.4
Zy2 - 30°C | 4.6849 | 5.1781 | 6.9 | 7.6 | 9 | 7.6
Zy4 - 50°C | 4.274 | 4.1918 | 7.1507 | 8.8767 | 7.8904 | 11 | 8.4 | 10.8 | 12.4 | 16.5 | 14.5
Zy2 - 50°C | 7.6438 | 9.1233 | 11 | 12 | 12.6 | 13.2
Zy4 - 80°C | 7.5616 | 8.0548 | 11.589 | 13.8082 | 14.3014 | 18 | 17 | 20 | 19.4
Zy2 - 80°C | 11.0959 | 12.8219 | 18 | 19 | 19.6 | 22
Tests in NaOH pH 12.5 ; Kato et al., 2013
T (°C) | 0 – 2 years | 1 – 2 years | 2 – 5 years
30 | 4 | 1.0 | -
50 | 6 | 2.0 | 1.3
80 | 10 | 2.2 | -
Corrosion rate (nm.y-1)
In the absence of complexing agents:
CR decreases with time=> Passive material
Low CR at low T
Only pre-transition regime investigated (oxide th< 2.5 µm)
H pick-up ratio in pure water and NaOH solution pH 12.5 Kato et al., 2013
Notes: Test performed by measuring H generation
Zy2 and Zy4 are equivalent in terms of corrosion behaviour

## Slide 13: WP3 session
C-14 inventory in irradiated Zr (M.HERM – KIT)
Leaching tests and corrosion measurements for irradiated Zr (C. BUCUR – RATEN ICN)
Analytical strategy to measure C-14 released from irradiated Zr (T.SUZUKI - SUBATECH)
Corrosion rate measurements on Zr-4 in alkaline media (S.CAES - SCK.CEN)
WP3 Summary and conclusions (S.NECIB – Andra)
Corrosion of Zirconium alloys and C-14 release from compacted waste (A.AMBARD – EDF)

## Slide 14: WP3 Summary
Materials : All
Inventory measurements:
  Experimental KIT, RATEN ICN, RWMC
  Modelling KIT, RATEN ICN, RWMC, SCK.CEN
Leaching experiments at room T and up to 80°C:
  NaOH solution : CEA, RATEN ICN, RWMC
  Ca(OH)2 solution : SCK.CEN
C-14 analyses:
  Inorganic / organic partition: CEA, RATEN ICN, RWMC, SCK.CEN, SUBATECH
  Speciation : CEA, SUBATECH, SCK.CEN
  Quantification: CEA, RATEN ICN, SCK,CEN, SUBATECH
Corrosion rate measurements:
  Electrochemistry : RATEN ICN, SCK.CEN
  Hydrogen measurements: RWMC
  C-14 release fraction: RWMC
IRF: RWMC

## Slide 15: Available Materials
Unirradiated Zr
  Oxide-free samples
  Pre-Oxidised samples (up to 3 µm thick)
Irradiated Zr
  Various Burn-ups:
  Oxide up to several 2.7 - 25 µm thick
  Metallic samples
  Outer oxide samples
Zr-2 | Zr-4 | M5TM | Zr
Zr-2 | Zr-4 | M5TM
  7 < BU < 100 GWd/tHU

## Slide 16: Materials Characterisations Unirradiated Zr
Unirradiated Zr-4 before testing (RWMC)
Pre-oxidised unirradiated Zr-4 (Oxide thickness = 2.7 µm) RATEN ICN
SEM (BSE mode) of an unirradiated Zr-4 (dislocation density: 4.1×1013/m². (SCK.CEN)
Laves phase (precipitates: Zr(Fe,Cr)2)

## Slide 17: Materials Characterisation Irradiated Zr
Top : Outside oxide layer along the
spent fuel cladding
Zr-4 (CANDU)
Down: Hydride (RATEN ICN)
SEM images for irradiated Zr-2 (BWR STEP III) before corrosion (2.7 µm)
(A) Bright field and (B) dark field micrographs of the radiation induced defects in the cladding. (C) High resolution micrograph of a radiation induced dislocation loop.

## Slide 18: C-14 Inventory
=> Good agreement between modelling and experiments
Organisations | Zircaloy Type | N content (ppm) | Burnups GWd/ThU | Inventory Modelling (Bq/g) | Inventory Experiments (Bq/g) | Gas/Liquid
KIT | Zr-4 | 50 | 50.4 | 3.5 ±0.4×104 | 3.7 ±0.4×104 | 90/10
RATEN ICN | Zr-4 (CANDU) | 30 | 7.5 | 1.78×104 | 2.12 ±0.3×104 | 99/1
SCK.CEN | Zr-4 | 17-25 | 60 | 1.3-1.9 ×104 |  | -
RWMC | Zr-2 | NA | 34 - 41 |  | 1.5 -3.5×104 | -
 | Zr-2 metal Zr-2 outer oxide |  |  |  | 2.5×104 5×104 | -
NAGRA (CEA) | Zr-4 M5TM | 34 27 | 54.50 46.57 |  | 1.78 ×104 3.03 ×104 | -

## Slide 19: Leaching experiments C-14 release in alkaline solutions
Solutions | T | pH | Durations | Organisations
NaOH (deaerated) | Room T 50°C 80°C | 12 – 12.5 | 14 days 3 months 6 months 10 months 12 months 18 months 2 years 5.5 years 6.5 years | CEA RATEN ICN CEA, RATEN ICN RATEN ICN RATEN ICN RATEN ICN RWMC RWMC RWMC
Ca(OH)2 (deaerated) | Room T | 12.5 | 6 months | SCK.CEN

## Slide 20: C-14 analyses Irradiated Zr (metal + oxide)
Organisations | Inorganic (%) | Organic (%) | Durations | Materials
CEA | 55 80 | 45 20 | 14 days & 6 months | M5TM Zr-4
RATEN ICN | 40 | 60 | 18 days – 18 months | CANDU Zr-4
RWMC | 30 | 70 | 6.5 yrs | Zr-2
=> Organics > Inorganics except for CEA

## Slide 21: C-14 analyses Irradiated Zr
=> Decrease of the gas content with time (only 7% after 5.5 years)
=> Increase of the organic fraction in the liquid phase

## Slide 22: C-14 analyses
Organisations | Speciation |  |  |  | Method
 | Solutions | Organics | Inorganics | Gas | 
CEA | NaOH | Glycolate Acetate Formate Oxalate | Carbonate |  | Anionic Chromatography
 | Blank | Acetate Formate | Carbonate |  | Anionic Chromatography
SCK.CEN | Ca(OH)2 | Acetate Formate |  | Methane Ethene CO2 | Ion Chromatography Gas Chromatography
SUBATECH | NaOH | Formate Acetate Propionate Oxalate |  |  | Ion Chromatography
Zr type does not influence C-14 speciation (Zr-4 + M5TM)
Some differences for CEA + SUBATECH => Difficulty of the analyses
Liquid phase=> Carboxylic acids + Carbonates
Gas phase => Hydrocarbons + CO2

## Slide 23: C-14 analyses Quantification
Organisations | Durations | Materials | Organic (Bq/g) | Inorganic (Bq/g) | Method
CEA | 14 days and 6 months | M5TM | 101 ± 10 | 110 ± 10 | LSC
RATEN ICN | From 18 d to 18 mths | Zr-4 (CANDU) | 7 ± 1.0 | 4.0 ± 1.0 | LSC
RWMC | 5.5 yrs | Zr-2 (Metal + Oxide) Metal | 0.49 0.14 |  | LSC

## Slide 24: Corrosion rate measurements
Organisations |  | Corrosion rate (nm/yr) |  |  |  |  | 
 | Materials | Durations | Unirradiated |  | Durations | Irradiated | 
Methods |  |  | H2 meas. | Electrochemistry |  | C-14 leaching fraction | Electrochemistry
RATEN ICN | Zr-4 (CANDU) Oxidised As-received Cut at one end | 12mths |  | 0.3 110 60 | 6 mths 18 mths |  | 110 50
RWMC | Zr-2 | 2 yrs | ~5 |  | 6.5 yrs | ~ 1 | 
SCK.CEN | Zr-4 |  |  |  | 6 mths | 84 | 
=> Decrease of the CR with time
Influence of irradiation on the CR
Significant uncertainties on the measurements (various techniques,…)

## Slide 25: Materials Characterisations
Unirradiated Zr-2 in NaOH solution (pH 12.5)
=> Oxide thickness increases with temperature
=> Monoclinic structure is not confirmed

## Slide 26: Materials Characterisation Irradiated Zr
Rinsing with HNO3 did not influence the oxide structure
=>The leaching experiments
did not modify the oxide microstructure

## Slide 27: Mechanisms
Congruent release with the CR=> to be clarified
Dissolution of ZrO2: Unlikely at alkaline pH
Oxide defects (cracks)
IRF (RWMC) estimated below 10% (between 3.5% and 7.5%) (based on oxide thickness data and ORIGEN-calculation)

## Slide 28: Main Conclusions
Inventory
  Good agreement between modelling and experiments
C-14
  Challenge to measure C-14 measurements : Very highly sensitive techniques needed
  C-14 activity is concentrated in the oxide (RWMC)
  Liquid phase> More organics (mainly carboxylic acids)
  Evolution of the speciation with time
Corrosion rate:
  Low CR measured experimentally; uncertainties of the measurements=> H2 meas. More accurate
  Congruent release of C-14 with the CR is not confirmed
  Difference between unirradiated and irradiated materials
  No evidence of a potential influence of the Zr type on the CR at low T
  Chloride seems to increase the CR
Mechanisms of C-14 release
  Fast release of C-14=> No significant evolution of the release concentration between 14 days and 18 months
  Oxide slows down the corrosion kinetics
  Based on the corrosion-related congruent release, the oxide layer is dominant in the 14C release
  Low IRF << 20%
  Migration of C-14 is unlikely (see A.AMBARD’s presentation)

## Slide 29: Outlook
AMS analyses ongoing to quantify organic molecules (CEA + PSI + SUBATECH)
Outstanding issues
  C-14 released as gas, as inorganics?
  From a SA point of view, It is needed to better understand the radionuclide leaching behaviour from the oxide layer
  Role of the inner oxide on C-14 release
  Long term experiments on various Zr type

## Slide 30
Thanks to all the CAST participants!