## Slide 1: 14C Content and Specification of SIERs from BWR
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
C. Rizzato, A. Bukaemskiy, N. Shcherbina
Forschungszentrum Jülich GmbH
EC CAST (CArbon-14 Source Term) Project

## Slide 2: Contents
Introduction and sample selection (T.4.1)
14C in SIERs (T.4.2):
  Analytical approach
  Total 14C content and speciation
  Morphological features of SIERs
14C released from SIERs (T.4.3):
  During leaching
  During storage
Effects of 𝛾-radiation and theoretical approach:
  Model 𝛾-irradiation experiments with IERs
  Benchmarking of experimental and model results
Conclusions
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 3: Introduction and sample selection
Sample selection criteria:
  Samples of SIERs from two different NPP were collected (FZJA, FZJB);
  𝛾-activity limitation;
  Different storage times (FZJB).
[Wolff. 2012]
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 4: Analytical approach: 14C content and speciation in SIERs (Task 4.2)
Sequential stripping of exchangeable and non-exchangeable 14C-fractions with quantification by LSC and HPLC. The remaining fraction associated with particulate matter is investigated by SEM.
Acidification
Combustion
Wet Oxidation
14C retained on SIERs
Exchangeable
Non-exchangeable
Inorganic
HCO3-, CO32-
Organic
HCOO-,CH3OO-
Particulate matter
Organic
CxHyOz
LSC (quantification)
HPLC (speciation and quantification)
SEM
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 5: Total 14C: combustion vs. sequential stripping (Task 4.2)
Sample: FZJA
Method for total 14C: Combustion with oxidation of released species
Method for inorg./org. 14C: Acidification and wet oxidation
Total 14C: 1770 ± 286 Bq/g
Inorganic 14C: 1900 ± 256 Bq/g
Organic 14C: 6.3 ± 0.4 Bq/g
Good reproducibility of results on total 14C and speciation
Inorganic and organic fractions of 14C were 99.6 % and 0.4 % respectively
The difference could be explained by the presence of a small fraction of particulate matter or by sample inhomogeneity
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 6: 14C inventory and speciation in SIERs (Task 4.2)
Chart: 
| FZJB-1 | FZJB-2 | FZJB-3 | FZJB-4 | FZJA
Inorganic | 0.994 | 0.989 | 0.995 | 0.991 | 0.996
Organic | 0.06 | 0.011 | 0.05 | 0.09 | 0.04
Inorganic 14C fractions ranges from 99.6 % to 98.9%
Organic 14C fraction ranges from 0.4 to 1.1%
No particular trend in 14C speciation depending on SIERs age and origin
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 7: 14C inventory and speciation in SIERs (Task 4.2)
Formic acid detected in small amounts (∼µg/gresin) (after regeneration)
Acetic acid – below detection limit
Sample FZJA: HPLC results
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018
Formic acid
Injection peak
Ghost peak
Acetic acid

## Slide 8: Morphological study (Task 4.2)
Agglomerates containing Fe and Co were observed with SEM/EDX
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018
Co
Fe
FZJB
Co
Carbon

## Slide 9: Morphological study (Task 4.2)
Agglomerates containing only Fe were observed with SEM/EDX
FZJB
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018
EDX-signal

## Slide 10: 14C release from SIERs (Task 4.3)
Main factors influencing 14C release:
  Acid-base equilibrium in the solution
  Effect of service/storage temperatures and/or strong oxidants (thermal/chemical degradation)
  Radiolysis: most -emitters in cation exchange fraction
  Bacterial growth: conversion of inorganic 14C into organic or produce anions that will displace 14C from the resins
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 11: 14C release: leaching in high pH solutions
Release of 14C in the gas phase is a result of a transient conditions: (local) pH decrease due to the release of H+ from the cation-exchange resins
On certain SIERs/XOH ratio CO2 may be released
pH evolution
On-line release of volatile 14C from SIERs in cementitious env.
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 12: 14C release: storage (Task 4.3)
Release of 14C: fast kinetics, influenced by equilibrium with atmospheric CO2
Enhanced release at elevated temperature: degradation of QA-groups
Self-irradiation effects on BWR SIERs was not observed on the laboratory time-scale
Release of 14C at RT
Release of 14C at RT and 50°C
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018
At T = 20ºC FR, % = 0.77 ± 0.02
At T = 50ºC FR, % = 1.5 ± 0.5

## Slide 13
0.1, 0.5, 1 MGy
Model γ-irradiation of IERs (Task 4.3)
Residual exchange capacity
NH3
HCOOH
CO32-
TMA
H2
C2H6
C3H6O
C3H8
Released species in solution & gas phase
De-amination and de-methylation are the preferred degradation mechanisms
De-amination causes decrease in salt-splitting capacity, de-methylation – increase of non-salt-splitting capacity;
Decreasing of salt-splitting capacity may promote a release of 14C as 14CO2
Irradiated model IERs
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018
g, air

## Slide 14: Benchmarking of experimental and model experiments
SIERs
𝛾-irradiated IERs
Common findings: H2, CO2, formic and acetic acids, TMA
Theoretical modeling (in progress)
Main degradation mechanism - de-amination, which provides for the loss of exchange capacity and release of 14CO2 fraction
Theoretical modelling (MD) is in progress to identify other accompanying processes
Some unidentified organic species
C2H6
C3H6O
C3H8
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 15: Conclusions
14C is present in BWR SIERs mainly in inorganic form (98.9 - 99.7%); organic fraction ranges from 0.4 to 1.1%; agglomerates of particulate matter were identified;
One of identified organic species is formic acid (exchangeable fraction);
Release of volatile 14C occurs during storage, increased at high temperatures; when SIERs are in contact with an alkaline solution, transient pH conditions result in the release of volatile 14C;
Ageing and radiolytic effects on BWR SIERs were not observed on the laboratory time-scales;
Model experiments of 𝛾-radiation on IERs demonstrated a release of H2, CO2, formic acid and QA-fragments, which is in agreement with the results for SIERs; the main degradation mechanism was proposed to be de-amination, which may provide for the loss of exchange capacity and release of 14CO2;
The results were obtained for unconditioned SIERs. The behaviour of e.g. cemented SIERs or other waste forms is likely to be different in repository-relevant conditions.
A. Bukaemskiy, N. Shcherbina, C. Rizzato – Final CaST Symposium – 16-18/01/2018

## Slide 16
Thanks
For Your Attention