## Slide 1: CArbon-14 Source Term CAST
The project has received funding from the European Union’s European Atomic Energy Community’s (Euratom) Seventh Framework Programme FP7/2007-2013 under grant agreement no. 604779, the CAST project.
Name: C. Bucur, I. Florea, R. Dobrin, D. Bujoreanu
Organisation: RATEN ICN Pitesti
Date: 17.01.2018
14C Content and Speciation of SIERs from CANDU

## Slide 2
RATEN ICN involvement in CAST WP4
SIERs sample available for experimental activities
Total 14C measurement
Inorganic & organic 14C measurement
Conclusions
Outlines

## Slide 3
3
Task 4.1: Current status review of 14C and its release from SIERs
Task 4.2: 14C Inventory and speciation in SIERs
  total 14C content in MOD&PHTS SIERs transferred from Cernavoda NPP (CANDU)
  inorganic/organic 14C
Task 4.3: 14C release from SIERs and its speciation
  liquid & gaseous 14C release under alkaline conditions from unconditioned CANDU SIERs: total 14C and inorganic/organic partitioning
  thermal degradation tests on CANDU SIERs
Task 4.4: Synthesis of experimental data and interpretation
RATEN ICN involvement in WP4
Results included in:
RIZZATO at al., 2014: CAST D4.1
RIZZO at al., 2017 – CAST D4.5
VEČERNÍK at al., 2017 – CAST D4.6
BUCUR at al., 2017 – CAST D4.7
D4.8: Rizzato et al., 2017 – CAST D4.8

## Slide 4: SIERs sample available for experimental activities
Origin of SIERs for CAST experiments:
MOD & PHTS of Cernavoda NPP - Unit 1 (sampled during maintenance operation)
Storage conditions: SIERs beads were collected and stored together
with small amount of heavy water (after ~19 y of operation HW contains ~ 0.6 TBq/kg of 3H)
SIERs transfer to ICN: July 2015 – 100 g SIERs diluted in demineralised water to get a D2O content less than 10% and decrease 3H content
The SIERs are stored under light water in three vaults made of reinforced concrete lined with eppoxy (200 m3/ each vault)
Neither sampling nor 14C measurement were performed before CAST on Cernavoda SIERs
Notes: during maintenance operation some spent resins beads are collected from the strainers of the purification systems and stored in drums. SIERs sampled from a drums with resins colected during meintenance operation was transferred to RATEN ICN in 2015 to be used in the experimental programme developed under CAST WP4. Since the SIERs collected during meintenance are not segregated depending on the provenience circuit, the sample transferred at RATEN ICN is a mixture of SIERs from purification systems of moderator (MOD) and of Primary Heat Transport System (PHTS) of Cernavoda Unit 1.

## Slide 5
Total 14C measurement

## Slide 6
Any hydrogen present is oxidized to H2O
Any carbon present is oxidized to CO2
Methodology - total 14C (1/2)
Non-catalytic combustion by flame oxidation method
SIERs samples (are combusted in an oxygen-enriched atmosphere with a continuous flow of oxygen using Sample Oxidizer, Model 307 PerkinElmer®

## Slide 7
  3H2O - condensed in a cooled coil, washed into a counting vial where it is mixed with LSC cocktail (Monophase®S)
  14CO2 - trapped by vapour-phase reaction with an amine (Carbo-Sorb® E ) and the resulting product (carbamate) is mixed with the LSC cocktail (Perma-fluor® E+) directly in the counting vial.
  At the end of the combustion cycle, two separate samples - a 3H sample and a 14C sample - are trapped at ambient temperature, minimizing the cross contamination.
14C and 3H activity is measured by LSC using Tri-Carb® 3110TR - allowing in ULL counting mode a count rate between 1‑20 CPM above the Bkg
Methodology - total 14C (2/2)

## Slide 8
Tests carried out using Amberlite IRN-150 labeled with 14C, 3H, 137Cs, 60Co, 241Am and 152Eu
The objective was to optimize the mineralization process with a total recovery of 14C and to check the possible cross contamination of the 14C sample with other beta emitters (specially 60Co and 137Cs)
Preliminary tests on labeled IER
14C recovery - 97.5% (93.8% - 99.9%)
MEM < 0.04%
No gamma emitters identified in the 14C vials
The optimal conditions for complete IER oxidation were selected:
  0.15 g of IERs (with water content of ~ 60% - similar with that of the real SIERs)
  ~ 0.5 ml combustaide
  ~ 3 min combustion time

## Slide 9
Total 14C measurement in CANDU SIERs
Gamma measurement on the sample resulted from SIERs sample combustion no gamma emitters were identified either in the counting vials for 14C measurement or in the 3H ones
# SIERs | SIERs mass, g | water content, % | Scintilator | 14 C activity, Bq/g
CANDU 1 | 0.149 | 60.10 | Permafluor E+ | 3.82E+04
CANDU 2 | 0.149 |  |  | 3.38E+04
CANDU 3 | 0.154 |  |  | 3.91E+04
CANDU 4 | 0.153 |  |  | 3.65E+04
CANDU 5 | 0.152 |  |  | 3.48E+04
 |  |  | Average | 3.65E+04
 |  |  | Stdev | 2.22E+03
  Combustion:
  Resin mass: ~ 0.15 g
  Water content:  = 60%

## Slide 10
Inorganic and organic 14C measurement

## Slide 11
Sequential extraction (combination of acid stripping and wet oxidation) from the same SIERs (A.Magnusson et all., 2008)
1st step: Acid stripping – inorganic fraction of 14C
14CO2 is absorbed in the first set of alkaline washing bottles
2nd step: Wet oxidation – organic fraction of 14C
K2S2O8 and AgNO3 combined with heating (~95C)
organic 14C are decomposed and it is absorbed in a second set of alkaline washing bottles placed after the catalytic furnace
catalytic furnace (holding Pt + CuO catalyst inside a quartz tube) – for complete oxidation of any reduced 14C compounds
Inorganic/organic 14C
  vacuum of - 0.2 bar: to avoid any gas release from the system
  N2 carrier gas : flow rate 60 - 80 ml/hour

## Slide 12
Preliminary tests for 14C recovery (1/2)
  IER (IRN-150) labeled with:
    inorganic 14C: Na2CO3/ NaHCO3
    organic 14C: CH3COONa and CH3-(CH2)10-COOH
    3H: HTO
     emitters: 137Cs, 60Co, 241Am and 152Eu
    129I: KI
  To optimize the experimental conditions and chemicals used
  To assess the 14C recovery
  To evaluate the reproductibility of the method
Notes: Since SIERs could contain beside 14C also tritium, iodine and other beta emitters that interfere with 14C measurement by LSC the gas washing lines consists in iodine traps (both before and after the catalytic furnace) with silver nitrate (AgNO3), slightly acidic trap with sulphuric acid (5% H2SO4) for absorption of the tritium and other potential interfering radionuclides and four alkaline traps (two placed before the catalytic furnace and two after it) with 2M sodium hydroxide (NaOH)

## Slide 13
Preliminary tests for 14C recovery (2/2)
  Acid dissolution: 10 ml HNO3
  Wet oxidation: 10 K2S2O8 5% + 4 AgNO3 (3 cycles)
  inorganic 14C recovery: 98% (96 – 100%)
  organic 14C recovery: 96%
  MEM: < 1%
  reproductibility: the standard deviation of the results of six identical tests were below 15%
  good efficiency for 14C purification
    no gamma emitters identified in solution sampled from alkaline gas washing bottles

## Slide 14
Inorganic & organic 14C in CANDU SIERs
  SIERs sample was filtered
  SIERs humidity after filtration: 60.10 % (mass loss by drying at 105C)
  Both SIERs and free water samples were analyzed
  SIERs sample
  Reaction vessel:
  1 g of wet SIERs
  0.2 g of carrier (Na2CO3 and CH3COONa)
  20 ml of NaOH 2M
  Liquid sample
  Reaction vessel:
  10 ml of water resulted from SIERs filtration
  0.2 g of carrier (Na2CO3 and CH3COONa)
  10 ml of NaOH 2M
  Acid stripping: 10 ml 6M H2SO4
  no heating
  1 hour
  Wet oxidation: 10 ml K2S2O8 5% + 4 ml AgNO3 4%
  3 cycles / 1 hour
  heating - 95C
  Acid stripping: 20 ml 6M H2SO4
  no heating
  1 hour
  Wet oxidation: 10 ml K2S2O8 5% + 4 ml AgNO3 4%
  3 cycles / 1 hour
  heating - 95C

## Slide 15
Inorganic & organic 14C in CANDU SIERs
Sample # | Bq/g in wet SIERs ( = 60%) |  |  | % in wet SIERs | 
 | Inorganic 14C | Organic 14C | Total 14C | Inorganic 14C | Organic 14C
CANDU 1 | 2.99E+04 | 3.44E+03 | 3.33E+04 | 89.68 | 10.32
CANDU 2 | 3.04E+04 | 1.88E+03 | 3.23E+04 | 94.18 | 5.82
CANDU 3 | 3.27E+04 | 2.04E+03 | 3.47E+04 | 94.12 | 5.88
CANDU 4 | 3.25E+04 | 2.00E+03 | 3.45E+04 | 94.19 | 5.81
CANDU 5 | 3.17E+04 | 2.18E+03 | 3.39E+04 | 93.56 | 6.44
average | 3.14E+04 | 2.31E+03 | 3.37E+04 | 93.15 | 6.85
stdev | 1.49E+03 | 6.42E+02 | 1.23E+03 | 1.96 | 1.96
Total 14C by combustion (0.15 g of SIERs) | average | 3.65E+04
 | stdev | 2.22E+03
SIERs free water Bq/ml | 
inorganic 14C | organic 14C
0 | 4.42
no inorganic 14C in the free water
very low organic 14C in free water (~0.01% from total 14C content in SIERs)

## Slide 16
Conclusions
  high amount of 14C was measured in CANDU SIERs (MOD&PHTS)
  3.6E4 Bq/g of wet SIERs ( = 60%)
  14C CANDU SIERs is predominantly as inorganic species
  ~ 93% as inorganic 14C
  ~ 7% as organic 14C species
  low amount of organic 14C was found in the SIERs free water
  ~ 0.01% from the total 14C content of the SIERs
  no inorganic 14C was measured in the SIERs free water

## Slide 17
Thank you for your attention!