## Slide 1: CArbon-14 Source Term CEA/EDF contribution to WP4 Ion-Exchange Resins CAST final symposium Lyon 16th - 18th January 2018
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Name: J. Comte(1), S. Legand(1), L. Petit(2),
Organisation: CEA-DEN(1) / EDF-R&D(2)

## Slide 2
Use of Ion exchange resins in EDF - PWR reactor
EDF-SIERs are combination of cationic, anionic and/or mixed bed resins
Used for purification of the various circuits in various operating history
Discharge conditions criteria are usually chemical or radiochemical saturation
EDF-SIERs are classified as Low and Intermediate level Short Lived waste (LILW-SL)
Name | Power reactor unit (MWe) | Type of fuel | Received | Mass (g) | Dose rate
EDF-A | 1450 | UOX | 06/2014 | 10 | 15 µSv/h (10g)
EDF-B | 1300 | UOX | 02/2015 | 4*10 | 300 µSv/h (10g)
Origin of SIERs / Context
Huge dose rates heterogeneity : SIERs coming from different circuits with different storage delays (decay)
  Samples are representative of the waste before conditioning (not of the “final waste”)
  Samples are made of SIERs from different circuits depending on the sampling campaign
Origin of the sample *
EDF provided samples from different origins (power reactor units, fuels…)
Sampling of SIERs are made during the “Mercure” conditioning campaigns
=> conditioning of SIERs in an epoxy matrix resin encapsulation and shielded concrete packages
  * for more detail show WP4 - CEA poster

## Slide 3
Task 4-2- Determination of source term
Analytical method developments
Total 14C by combustion with O2
IER (0.2 to 0.5 g) mixed with carrier (graphite)
Combustion under O2 (25 bars)
CO2 produced by mineralization of resins :
  trapped in NaOH solution as CO32- into the mineralization device during combustion and cooling
  to achieve the recovery of 14C, system is degassed in a venting station and the gases are flushed into NaOH bubblers
Speciation of 14C by acidic mineralization
Sample + carbon carrier
Sodium hydroxyde solution (Inside)
  IER (0.2 to 0.5 g) spiked by carbonate solution (carrier)
  First step : measurement of mineral 14C
  Acidification by H2SO4
  Degassing under N2 and vacuum into NaOH bubblers
  Measurements of CO32- carrier (recovery) and 14C by LSC
Second step : measurement of organic 14C
  Concentrated acid (H2SO4/HNO3) with oxidant (H2O2)
  Degassing under N2 and vacuum reflux into NaOH bubblers
  Measurement 14C by LSC
Similar as « Magnusson method»
Combustion with O2 | 
14 C recovery | > 95 %
Acidic dissolution method 14C recovery and selectivity | 14C minéral | 14C organic
14C mineral | > 95 % | < 3 %
14C organic | < 6 % | > 90 %
Optimizations on virgin resins spiked with 14C as carbonate and/or glucose

## Slide 4: Task 4-2- Determination of source term Result
Analytical methods comparison
EDF-A sample : similar results between the combustion method and the acidic dissolution
EDF-B sample : inconsistent results between the two methods
Application of the method on dried samples
Measurements showed non reproducible results (H2O content variability / analytical problems)
Final results on WET samples
Sample | Type | Total 14C Bq.g-1 Combustion with oxygen | Total 14C Bq.g-1 Acidic dissolution | Difference
EDF – A | Wet | 5570 ± 430 | 5610 ± 430 | 40 Bq.g-1 (0.6%)
EDF –B | Wet | 2125 ± 200 | 1612 ± 150 | 513 Bq.g-1 (24%)
  Total carbon determined by combustion/ Organic form determined by acidic dissolution
  (*) Total carbon 14 not consistent between combustion method and acidic dissolution method
Origin | Sample | State | 14C Bq.g-1 | Mineral form | Organic form
UOx-1450 | EDF-A | Wet | 5570 ± 430 | 77% | 23%
UOx-1300 | EDF-B | Wet | 2125 ± 200 | Can not be determined (*) | 
  More experiments are needed
  Samples representativeness is questioned (→ statistical approach needed)
  Samples consist in SIERs from different circuits depending on the sampling campaign

## Slide 5
Desorption experiments performed to identify organic compounds fixed on the SIERs
Task 4-3 Desorption experiment to
identify organic compounds fixed on the SIERs
  Desorption ~1 g of wet SIERs by LiOH (1 mol.L-1) permits obtaining solutions with organic carbon-14 (from 2.103 to 2.104 Bq.L-1 )
  A complete program of characterization was performed :
  Total organic carbon : 50 mg.L-1 of total organic carbon were measured
  Carboxylic acids by anionic chromatography : Acetate & formate detected in (contamination), only glycolate comes from resin desorption (< 8 mgacid.L-1).
  Amines by cationic chromatography : No amine detected => no chemical degradation of functional groups observed in these experimental desorption experiments.
  Low molecular weight volatile molecules by Gas Chromatography – Mass Spectrometry => No volatile organic detected in solution
  Molecules with higher molecular mass by Electrospray – Mass Spectrometry : LiOH matrix observed but no organic compound with higher molecular weight detected (probably masked by salts signal)
  for more detail show WP4 - CEA poster

## Slide 6
Carbon 14 measurements : synthesis
Task 4-2 : Aim of the project achieved
Two analytical methodologies (combustion and acidic method) were developed for total 14C and speciation measurement. Methodologies were applied on real samples (Dry/Wet)
Results show
That it is difficult to compare different wet SIERs (H2O content variability / analytical problems)
14C speciation on one sample showing ~75 % of mineral carbon
But question remain about the representativeness of the results
=> Statistical approach needed
Task 4-3 : Aim of the project achieved
Desorption experiments permit obtaining aqueous solutions containing 14C in organic form for the determination of the hydro soluble organic compound with different techniques (IC, GC-MS, ESI-MS)
Results show
Only one organic compound representative of resin desorption is observed in this matrix (high concentration in salt and presence of pollution)
But doesn’t complete the carbon organic mass balance (~1 % of TOC identified)
Complementary studies (14C measurements, drying resins, desorption experiment) are needed but not compatible with the CAST project (delay, cost …)

## Slide 7
The authors thank the following people who participated to this project
LABORATORY OF RADIOCHEMICAL AND CHEMICAL ANALYSIS,
CEA, DEN, DEC, SA3C, LARC F-13108 Saint-Paul-lez-Durance, France
J. Comte (jerome.comte@cea.fr), A.L. Tornabene, J. Moinot, C. Point, M. Thouvenin
LABORATORY OF RADIOLYSIS AND ORGANIC MATTER
CEA, DEN, DANS, DPC, SECR, LRMO F-91191 Gif sur Yvette, France
S. Legand (solene.legand@cea.fr) , F. Casanova and D. Lebeau
With the support of
EDF R&D, Materials and Mechanics of Components Department
EDF Lab les renardieres F-77818 Moret Sur Loing, France
L. Petit (laurent-der.petit@edf.fr), G. Heisbourg
  for more detail show WP4 - CEA poster