## Slide 1: EC CAST (CArbon-14 Source Term) Project Cementation of SIERs and Consequences on C-14 mobility
The project has received funding from the European Union’s Seventh Framework Programme for research, technological development and demonstration under grant agreement no. 604779, the CAST project.
Petr Večerník
ÚJV Řež, a. s.
16th – 18th January 2018
CAST Symposium

## Slide 2
One of the goals of UJV work was to verify the using of the cement as a suitable matrix for SIERs solidification and study the leaching process on cemented samples.
Presentation outline:
real and artificial SIERs characterisation
14C tracers interaction with cement
resins fixation into cement matrix
leaching of cemented samples

## Slide 3
SIERs characterisation
real SIERs samples
Dukovany NPP (EDU), Temelín NPP (ETE)
ÚJV Group research reactor (UJV)
  all sampled in the past , lack on information
activity (Bq/g) | EDU | ETE | UJV
14C (total) | 48 ± 5.9 | 43 ± 4.0 | 2000 ± 280
14C (inorganic) | 14 ± 2.2 | 16 ± 2.0 | 2000 ± 280
14C (organic) | 34 ± 5.5 | 27 ± 4.0 | 77 ± 11
other major radionuclides: 40K, 51Cr, 60Co, 108mAg, 125Sb, 125I, 134Cs, 137Cs

## Slide 4
SIERs characterisation
artificial SIERs samples
Amberlite resins in OH and Cl form saturated by: sodium bicarbonate (NaH14CO3)
    sodium acetate (CH314COONa)
    - activity of 14C: 6.5 kBq/g of dry resin

## Slide 5
14C tracers interaction with cement
CEM II/A-S 42,5 R used as a fixation matrix
hardened cement paste crushed and sieved
(A: <0.1 mm; B: 0.1-0.5 mm)
batch sorption test in distilled water; L/S = 10
NaH14CO3 and CH314COONa
tracer only, tracer + carrier (10-5, 0.1 and 1 mol/L)
14C activity 2MBq/L in initial liquid phase

## Slide 6
14C tracers interaction with cement
sorption (interaction) of 14C bicarbonate on hardened cement paste
- due to conditions (high pH, presence of Ca2+ ions) precipitated as calcite
all (bi)carbonates immobilised in solid phase

## Slide 7
14C tracers interaction with cement
sorption (interaction) of 14C acetate on hardened cement paste (mesh A: <0.1 mm; B: 0.1-0.5 mm)

## Slide 8
resins fixation into cement matrix
CEM II/A-S 42,5 R used as a fixation matrix
cement/dry resin = 10/1
water/cement ratio= 0.6
cylindrical specimens: d= 26mm, h = 55mm

## Slide 9
leaching of cemented samples
- leachability index (Li)
ANSI/ANS-16.1-2003 Measurement of the Leachability of Solidified Low-Level Radioactive Wastes by a Short-Term Test Procedure
- diffusion coefficient (De)
 is a defined constant (1.0 cm2/s) and Di is the effective diffusivity (cm2/s) of radionuclide i calculated from the test data
an - the quantity of a nuclide released from the specimen during leaching interval n, A0 - the total quantity of a given contaminant in the specimen, (t)n - the duration of the nth leaching interval (s), V - volume of the specimen (cm3), S - geometric surface area of the specimen (cm2), T - leaching time (s)

## Slide 10
leaching of cemented samples
- based on ANSI/ANS-16.1-2003
leaching media: distilled water,
            0.02M NaOH
            SGW (synthetic granitic water)
            - liquid volume (V)/sample surface (S) = 10 or 5 and 2.2
ANSI/ANS-16.1-2003 Measurement of the Leachability of Solidified Low-Level Radioactive Wastes by a Short-Term Test Procedure

## Slide 11
14C bicarbonate, V/S = 10
pilot test - leaching into distilled water (DV)
liquid volume (cm3)/sample surface (cm3) = 10 (cm)
duration of 90 days
      negligible release of 14C during the test
      leachability index Li = 12.2
      diffusion coefficient De < 6·10-12 cm2s-1 (i.e. 6·10-16 m2s-1)

## Slide 12
14C bicarbonate, V/S = 5
leaching into distilled water , SGW and NaOH solution
liquid volume (cm3)/sample surface (cm3) = 5 (cm)
duration of 160 days

## Slide 13
14C bicarbonate , V/S = 5

## Slide 14
14C bicarbonate , V/S = 5
leaching into distilled water , SGW and NaOH solution
liquid volume (cm3)/sample surface (cm3) = 5 (cm)
duration of 160 days
      negligible release of 14C during the test
 | DV | SGW | NaOH
Li | 13.2 | 12.1 | 13.3
De (cm2s-1) | < 2.5·10-12 | < 7.0·10-12 | < 2.6·10-12

## Slide 15
14C acetate , V/S = 5
leaching into distilled water , SGW and NaOH solution
liquid volume (cm3)/sample surface (cm3) = 5 (cm)
duration of 124 days
      artificial SIERs in OH and Cl form

## Slide 16
14C acetate , V/S = 5
leaching into distilled water , SGW and NaOH solution
      big variance in obtained experimental data
form |  | DV | SGW | NaOH
OH | Li | 11.2 | 10.7 | 12.1
 | De (cm2s-1) | < 1.4·10-9 | < 3.8·10-9 | < 1.6·10-9
Cl | Li | 11.5 | 11.3 | 10.9
 | De (cm2s-1) | < 4.5·10-9 | < 1.5·10-9 | < 1.3·10-9

## Slide 17
14C acetate , V/S = 2.2
leaching into distilled water , SGW and NaOH solution
liquid volume (cm3)/sample surface (cm3) = 2.2 (cm)
duration of 124 days
      artificial SIERs in OH and Cl form

## Slide 18
14C acetate , V/S = 2.2
leaching into distilled water , SGW and NaOH solution
      big variance in obtained experimental data
form |  | DV | SGW | NaOH
OH | Li | 11.1 | 11.2 | 11.6
 | De (cm2s-1) | < 1.7·10-9 | < 7.1·10-8 | < 9.5·10-10
Cl | Li | 11.1 | 10.5 | 11.0
 | De (cm2s-1) | < 2.4·10-9 | < 1.7·10-9 | < 1.3·10-9

## Slide 19
  negligible/no inorganic 14C leaching from cemented resin
  very low organic 14C leaching from cemented resin
  no significant influence of leaching media
  change of liquid phase amount had no effect on leached amount of 14C
results