## Slide 1
Ion irradiation used as surrogate for neutron irradiation to understand nuclear graphite evolution during reactor operation: consequences for the long lived radionuclide’s behavior
N. Toulhoat1,2 , N. Moncoffre1, Y. Pipon1, N. Bérerd1
1 Université de Lyon, CNRS/IN2P3, IPNL, France
2 CEA Centre de Saclay, France
1

## Slide 2
Task 5.2: Develop approaches to characterise the 14C inventory in
irradiated graphites
Partner n° 28 CNRS/IN2P3 (IPNL)
Study the effects of neutron irradiation on the behaviour of 14C and provide information on 14C distribution, chemical state and release after reactor shutdown
Virgin nuclear graphite or model graphite (HOPG)
13C or 36Cl implanted : simulate 14C displaced from its original
structural site through recoil
Ion irradiation : simulate neutron irradiation
Same job on 36Cl
(T1/2 ~ 300 000 years, released due to the mobility of Cl- in clay host rocks)
2
Our aim

## Slide 3
13C
14N
14C issued from 14N
14N(n,p)14C
(mainly close to pores 14N is adsorbed during maintenance cycles)
released by radiolytic corrosion (in CO2 cooled reactors)
14C issued from 13C
13C(n,g)14C
(mainly in the bulk)
stable up to T ~ 1600°C
What we already know on 14C and 36Cl in nuclear graphite
14C : two different origins inducing contrasted locations
G. Silbermann et al. Nuclear Instruments and Methods in Physics Research Section B 332 (2014) 106 -110
N. Moncoffre et al. Journal of Nuclear Materials 472 (2016) 252-258
36Cl : mainly produced through the activation of 35Cl (nuclear graphite impurity) 35Cl(n,g)36Cl
36Cl located at crystallite edges released from T = 200°C
36Cl located inside crystallites released at T > 1200°C
36Cl release related to the structure of graphite
C.E. Vaudey et al. Journal of Nuclear Materials 395 (2009) 62-68
C.E. Vaudey et al. Journal of Nuclear Materials 418 (2011) 16–21
A. Blondel et al. Carbon 73 (2014) 413-420
N. Toulhoat et al. Journal of Nuclear Materials 464 (2015) 405–410

## Slide 4
Question : Behavior of 14C and 36Cl during reactor operation?
Impact of neutron irradiation + temperature on the 14C and
36Cl behavior?
How does irradiation modify the graphite structure
How does the structure modification influence the
radionuclides release?

## Slide 5
Ion implantation
37Cl or 13C implantation to simulate 36Cl or 14C
Implantation
HOPG model graphite
Nuclear graphite
Binder
(made of coal tar pitch)
Filler
(Coke grain )
Pore
~ 80%
37Cl
37Cl (at.ppm)
13C (at.%)
Depth (nm)
13C
3x1013 37Cl.cm-2 ~ 25 ppm
6x1016 13C.cm-2 ~ 4 at.%
Less ordered
Well ordered
Highly Ordered Pyrolytic Graphite HOPG to simulate coke grains
37Cl or 13C implantation to simulate 36Cl or 14C
(measured by SIMS)

## Slide 6
Two different structural states
ID1/IG and FWHMG parameters : monitor the graphite structure disorder
Implantation alows simulating two different structural states :
G mode : planar vibrations of C atoms
D mode : hetero-atoms, vacancies, grain boundaries and other defects
less disordered
highly disordered

## Slide 7
Ion irradiation to simulate neutrons
Neutrons generate atom displacements producing mainly Ballistic damage (1 - 3 dpa)
Recoil carbon atoms transfer some energy through excitations and ionisations
Nuclear stopping power (Sn) + Electronic stopping power (Se)
Stopping power (Stot) =
Ballistic regime is favored
Electronic regime is favored
Ions used to simulate neutron irradiation effects
Method
Method

## Slide 8
Structure evolution
Electronic
Ballistic
Ballistic irradiation (dpa >> 1) : strong disordering
compensated by temperature annealing effects
Electronic regime or ballistic at low dpa level : almost no impact on disordering
Less disordered structure through implantation
3D reordering
In plane reordering

## Slide 9
Structure evolution
Highly disordered structure through implantation
Temperature alone or electronic regime : no impact
Ballistic irradiation + temperature : three dimensional
reordering of the structure
Increase of the size of the coherent domains
HRTEM and squeletonized images

## Slide 10
Athermal radiation enhanced annealing process
(break-up of clusters and vacancy-interstitial
annihilation)
Higher Ea values reported in the literature to achieve three dimensional temperature reordering
10
Highly disordered structure through implantation
Reordering process
Ea ~ 0.09 eV
FWHM irradiated
FWHM unirradiated
D FWHM =
Very low reordering activation energy

## Slide 11
Ar+ Irr. 200°C
Ar + Irr. 500°C
Ar + Irr. 1000°C
C + Irr. 500°C
37Cl release under irradiation
Argon ions
Argon irradiation (dpa >> 1) break the graphene planes
37Cl at broken crystallite edges is released

## Slide 12
13C might be stabilized into new
formed carbon clusters?
Almost no 13C release
whatever the
irradiation conditions
13C release under irradiation

## Slide 13
Irradiation (ballistic
damage) +
Temperature
Favor 14C incorporation into new carbon structures
Favor 36Cl release (more than 30% released in hot and highly irradiated areas)
Inferred behavior for 14C and 36Cl in irradiated graphite
Nature and initial structural state (binder, coke), irradiation history and position of graphite in the reactor will lead to significant structural heteroneneities
-
-
-
-
-
-
Depleted 36Cl zones
High temperature annealing (T > 1300°C) prior to disposal should in any case be beneficial
To stabilize 14C
To release 36Cl bound to edge planes (which should be more accessible to leaching)

## Slide 14
This presentation is mainly based on results issued from the PhD of N. Galy (2013 - 2016)
Our results are also the fruit of cooperation with
M.R Ammar and P. Simon from CNRS/CEMHTI Orléans, France
J.N. Rouzaud and D. Deldicque from Ecole Normale Supérieure , Groupe de Géologie, Paris, France
P. Sainsot from Université de Lyon, INSA-Lyon, France

## Slide 15
The authors are very grateful to
The European (Euratom) Programme FP7/2007-2013 under the grant agreement n° 604779 (CAST 14)
Technical support
Financial support
IPNL accelerator staff (VDG 4MV and IMIO 400)
ICUBE laboratory, Strasbourg University
TANDEM accelerator staff, Orsay
CEMHTI accelerator staff, Orléans
Thank you for your attention !