## Slide 1: Carbon-14 release from Oldbury graphite. Use of experimental results to inform the safety case
Steve Swanton
CAST Symposium, Lyon, 17 January 2018

## Slide 2
Inventory of C-14 in UK graphite
2012 assessment of gas phase C-14 release
Leaching of Oldbury graphite
  samples
  experimental details
  results up to one year
Enhanced model for C-14 release (2015)
Further leaching results up to 30 months
  comparison with model
Conclusions
Outline

## Slide 3
Irradiated graphite provides the largest inventory of carbon-14 associated with irradiated material in UK ILW
Core graphite makes up large fraction of graphite wastes by mass and contains most of carbon-14
Other graphite contains much less carbon-14
Carbon-14 in graphite in UK Waste Inventory
Graphite to be disposed to cement-based geological facility

## Slide 4
First order release from graphite (i.e. rate proportional to activity remaining in graphite), independent of geometry, conditions, etc.
  Rate constant 5×10-4 yr-1
All of carbon-14 inventory can be released
All carbon-14 released as 14CO2 or 14CH4 into surrounding grout
  Speciation 99% CO2, 1% CH4 (based on very limited data)
CO2 captured as carbonate, so only carbon-14 in CH4 released as gas
Previous assessment model for C-14 (2006)

## Slide 5
Indicate carbon-14 release from core graphite provides substantial contribution to total carbon-14 release
  Peak release rate 0.03 TBq/year
  Operational dose is 0.5 µSv/year
    This is below design target (10 µSv/year) and small compared to release from other wastes
Post-closure annual risk is 5×10-5 using simple potentially very cautious approach (no geosphere, minimum release area)
  This is significantly above the target (10-6)
Substantial uncertainties in data
Release from graphite represented using very simple model
2012 Gas assessment results

## Slide 6
Improve understanding of the release of carbon-14 from graphite by
  Generating new experimental data and analysing existing data
    to identify relevant factors in the release (e.g. conditions, speciation, fraction releasable, time evolution of release)
    Updating modelling to represent relevant factors
So that
  Uncertainties in calculations can be reduced
    Either calculated release rate is reduced below targets
    Or investment in determining alternative solution to issue is better justified
Aims of RWM programme on graphite

## Slide 7
Cylindrical spacer piece from an installed set
  90mm long, 70mm diameter, 300g mass
Removed from Oldbury Reactor 2 in 2005 after 38 years service
Oldbury (Magnox) graphite samples

## Slide 8
Sub-samples from outer surface (2) and cut faces (2) analysed for radionuclide content
        Reference date: 19 December 2011
Graphite sample inventory

## Slide 9
6 gas-phase release experiments
  Analysis for 14CO2, 14CO (volatile oxygenated organics) and 14C-hydrocarbons in gas phase
Additional solution leaching experiment
Leaching experiments (Phase 1)

## Slide 10
Leaching experiments
30g intact samples leached in NaOH solution pH 13
For anoxic tests, de-aerated water equilibrated with iron foil was used
Handling in N2 atmosphere
Gas phase purging system

## Slide 11
Samplers are evolutions of dry-bed absorber systems developed for 3H, 14C and 35S speciation studies of discharges from nuclear establishments
Series of soda lime and silica gel columns to collect CO2 and H2O
  Unit 1 - collects gas phase 14CO2 and 3H2O
  Unit 2 - oxidation of H2 and CO to H2O and CO2 by CuO catalyst, 350°C
  Unit 3 - oxidation of organic compounds to H2O and CO2 by Pd catalyst, 425°C
Gas phase carbon-14 analysis

## Slide 12
Purge reactor headspace with nitrogen
  near-quantitative collection of all gas phase species
  collection columns returned to RCD for analysis
CO2 is extracted from columns converted to benzene for 14C analysis by LSC
  LoD 0.01 to 0.03 Bq 14C per sample
Solution phase samples were analysed by pyrolyser and LSC for total 14C
  organic 14C, samples were acidified to remove carbonate fractions before pyrolysis/LSC
Carbon-14 analysis

## Slide 13
Ratio organics to CO
  1:1 in oxic conditions
  2.5:1 in anoxic conditions
Negligible 14CO2 in gas phase
Speciation of gas phase carbon-14

## Slide 14
Carbon-14 release to solution – anoxic pH 13

## Slide 15
Carbon-14 release, anaerobic, pH 13

## Slide 16
Fast initial release of carbon-14 on immersion in water
The rates of 14C release decreased with time
Most of the 14C released remained in the aqueous phase
~1% of the carbon-14 released was as volatile gaseous species
Gas phase speciation depends in part on redox conditions
  1:1 hydrocarbons: CO under oxic conditions
  2.5:1 hydrocarbons: CO under anoxic conditions
Conclusions from experiments (to 1 year)

## Slide 17
Based on improved understanding from Oldbury graphite and other experimental studies (e.g. Carbowaste), enhanced empirical model developed
  Large proportion of carbon-14 remains unreactive and is not released
  Small proportion of carbon-14 released rapidly before repository closure
  Remaining proportion released at a slower rate that continues into repository post-closure period
  Release mainly into solution, with a small proportion released as gas
  Gas phase speciation (between 14C-hydrocarbons and 14C-O species) depends on conditions
Parameters estimated from latest experimental data
Enhanced assessment model

## Slide 18
Uncertainty (and variability) considered in parameterising model
Key values are:
Effect of uncertainty
Both best estimate and variant calculations performed

## Slide 19
Enhanced model substantially reduces calculated gaseous 14C release from graphite in long term
Enhanced model may still be cautious
Updated assessment model

## Slide 20
Resampling after further 18 months
Runs 2, 3 - baseline, intact, anoxic, high pH
Run 3b – baseline (solution only)
Run 5 – powdered sample, anoxic, high pH
Measured
  Gas phase C-14 (Runs 2, 3 and 5)
  Solution phase total C-14
  Solution organic C-14 (after acidification to remove inorganic C-14)
Leaching experiments (Phase 2)

## Slide 21
Longer-term 14C release – gas phase

## Slide 22
Longer-term 14C release - solution

## Slide 23
Majority of release is as 14CO2
Up to 30% 14C in organic fraction (intact samples)
Organic fraction of 14C in solution

## Slide 24
Comparison with enhanced model

## Slide 25
Fast initial release of carbon-14 occurs from Oldbury graphite on immersion in water
Rate of release decreases with time and is barely measurable beyond one year
Release predominantly as 14CO2, which is absorbed in alkaline solution; at high pH up to 30% as soluble organic species
Less than 1% of release occurs as volatile species to gas phase
Gas phase speciation depends in part on redox conditions
  1:1 hydrocarbons: CO under oxic conditions
  2.5:1 hydrocarbons: CO under anoxic conditions
Current assessment model may be cautious concerning carbon-14 release to gas phase
Future assessments will need to consider migration of organic C-14 species via the groundwater pathway
The baseline experiments are continuing…
Conclusions

## Slide 26
Carbon-14 Release from Oldbury Graphite, Amec Report AMEC/5352/002 Issue 3, 2014
Carbon-14 Project Phase 2: Irradiated Graphite Wastes, AMEC/200047/004 Issue 2, 2016
Available from https://rwm.nda.gov.uk/publications/
Further studies of Carbon-14 Release from Oldbury Graphite, due to be published in 2018.
References

## Slide 27
Graham Baston, for managing the experimental work
Steve Preston for graphite sample preparation
Mark Kirkham, Bijan Farahani and James Schofield for experimental maintenance and sampling
Ben Swift for modelling of 14C gas generation
Adrian Clacher for solution phase 14C analysis
Bob Otlett and Jill Walker (RadioCarbon Dating Ltd) for gas phase 14C analysis
This work was funded by Radioactive Waste Management Limited
Acknowledgements

## Slide 28
Thank you for listening
Any questions?

## Slide 29: Additional slides

## Slide 30: Comparison of enhanced model with experimental results

## Slide 31: Comparison of enhanced model with previous model

## Slide 32: Updated performance assessment results for shielded ILW vaults