## Slide 2
CAST Acknowledgement
For more information, please visit the CAST website at:
http://www.projectcast.eu
The project has received funding from the European Union’s European Atomic Energy Community’s (Euratom) Seventh Framework Programme FP7/2007-2013 under grant agreement no. 604779, the CAST project.

## Slide 3: Simon Norris
CAST WP5 Irradiated Graphite Main Outcomes

## Slide 4: Agenda
Work Package 5 - Graphite | 
11.00 - 11.10 | WP5 - Overview of Main Outcomes. Simon Norris (RWM)
11.10 - 11.35 | Ion irradiation used as surrogate for neutron irradiation to understand nuclear graphite evolution during reactor operation: consequences for long lived radionuclide behaviour. Nelly Toulhoat (IPNL)
11.35 - 11.55 | 14C in TRIGA Irradiated Graphite and its Release under Alkaline Conditions. Crina Bucur (RATEN ICN)
11.55 - 12.20 | Oldbury graphite study for RWM. Steve Swanton (Wood)
12.20 - 12.30 | WP5 Summary and Conclusions Simon Norris (RWM)
12.30 - 13.15 | Lunch & Poster Session
13.15 - 13.40 | New concept and instruments for 14C measurements in i-graphite. Gérard Laurent (Integrated Nuclear Engineering Solutions)
Deliverables freely available at https://www.projectcast.eu/

## Slide 5: Key generation and migration processes affecting the fate of C-14 in the disposal system

## Slide 6: WP5 Graphite
13 participants (RATEN ICN, ENRESA, FZJ, ENEA, Andra, EdF, LEI, IGNS, CIEMAT, CNRS/IN2P3, IFIN-HH, ALD-F, RWM)
8 countries represented – range of national approaches to irradiated graphite management (e.g. surface disposal, geological disposal)
Affects research requirements, prioritisation of i-graphite issues in national programme, and ‘size’ of required research programme
Led by RWM

## Slide 7: WP5 Programme – Deliverables (1)
Objective | Main Deliverables (Outcome) | Timing (Month, October 2013 was M1)) | Status
Determining the 14C inventory and concentration distribution in irradiated-graphites and factors that may control these | D5.1 Review on 14C leaching in French i-graphite | M8 | Achieved
 | D5.2 WP5 Annual Progress Report – Year 1 | M12 | Achieved
 | D5.3 Report on graphite categories in the RBMK reactor | M12 | Achieved
 | D5.4 Definition of the scientific scope of leaching experiments and definition of harmonised leaching parameters | M14 | Achieved
 | D5.5 Review of current understanding of inventory and release of 14C from irradiated graphites | M14 | Achieved
 | D5.6 WP5 Annual Progress Report – Year 2 | M24 | Achieved
 | D5.7 Report on 14C distribution in irradiated graphite from research reactor VVR-S using accelerator mass spectrometry and beta imaging | M24 | Achieved
 | D5.17 Report on modelling of 14C inventory in RBMK reactor core | M42 | Achieved

## Slide 8: WP5 Programme – Deliverables (2)
Objective | Main Deliverables (Outcome) | Timing (Month, October 2013 was M1)) | Status
Measure the rate and speciation of 14C release to solution and gas from irradiated-graphites in contact with aqueous solutions | D5.8 Synthesis report on 14C speciation in solution and gas from French graphite waste. | M26 | Achieved
 | D5.9 WP5 Annual Progress Report – Year 3 | M36 | Achieved
 | D5.10 Final report on 14C release and inorganic/organic ratio in leachates from TRIGA irradiated graphite | M40 | Achieved
 | D5.12 Final evaluation of leach rates of treated and untreated i-graphites | M45 | Achieved
 | D5.14 Release of C14 from irradiated VVR-S graphite to solution and gas phase | M45 | Achieved
 | D5.15 Final report on 14C leaching from Vandellos1 graphite | M45 | Achieved
 | D5.18 Report on 13C behaviour under ion irradiation in HOPG (model graphite) | M45 | Achieved
 | D5.19 Final report on results from WP5 | M46 | Achieved

## Slide 9: WP5 Programme – Deliverables (3)
Objective | Main Deliverables (Outcome) | Timing (Month, October 2013 was M1)) | Status
Determine the impact of selected waste treatment options on 14C release and relating this to the nature of 14C in irradiated-graphite. | D5.11 Report on exfoliation processes and on structural and morphological properties of treated graphites | M40 | Achieved
 | D5.13 Vandellos 1 graphite compilation report: thermal decontamination and IGM wasteform results | M45 | Achieved
 | D5.16 Report on effect of removal of surface layer of graphite on C14 release and behaviour of C14 in cement waste packages | M45 (June 2017) | Could not progress -samples unavailable, due to delay in implementation timelines regarding decommissioning of Chernobyl NPP

## Slide 10: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  RATEN ICN, Romania
  Title of report on CAST website
D5.10: Final report on C-14 release and inorganic/organic ratio in leachates from TRIGA irradiated graphite
  Key outcomes as presented in report
  Both for anaerobic and aerobic conditions, less that 2% from the initial 14C activity of the i-graphite subject to the leaching test was released
  The leaching rates are high in the first days of immersion and decrease after that, indicating a two stage process:
    an initial quick release for the first 48 days: less than 9E-02 % of inventory/day
    followed by a slower release rate: around 4E-3 % of inventory/day
  The ratio between inorganic and organic 14C release during the leaching test is almost constant
    more organic than inorganic 14C released under anaerobic conditions: an average fraction of organic 14C of around 65% from the total 14C released
    more inorganic than organic 14C released under aerobic conditions: an average fraction of inorganic 14C of around 68% from the total 14C released

## Slide 11: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  - CNRS/IPNL France
  Title of report on CAST website
  - D5.18: Report on 13C behaviour under ion irradiation in HOPG (model graphite)
  Key outcomes as presented in report
  - Ion irradiation at different temperatures of 13C (used to simulate 14C) implanted HOPG model graphite samples was used to simulate neutron irradiation
  - The structure modifications were followed by Raman microspectrometry and HRTEM and 13C was measured by SIMS
  - Temperature and irradiation have counteracting effects on the graphite structure evolution (irradiation disorders, temperature reorders)
  - Whatever the irradiation regime (ballistic, electronic), the implanted 13C is stabilized in graphite (sp2 or sp3 structures)
  - Extrapolation to 14C: Apart from the 14C formed by activation of 14N for which a great part has probably been removed through radiolytic corrosion, both temperature and irradiation tend to be stabilize 14C in the irradiated graphite structure

## Slide 12: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  - CIEMAT (Spain)
  Title of report on CAST website
  - D 5.15 Final report on 14C leaching from Vandellós graphite
  Key outcomes as presented in report
- Leaching test were carried out using deionized (DI) and synthetic water (SW) on sleeve graphite core samples of 11 mm x 12 mm (Ø x H)
  - The 14C avg. activity of the samples was 1,17E+04 Bq/g (Stdev. 8,74 %)
  - It has not been found in the leachates 14C above detection limits (2,4E-02)
  - Acetate, formate and oxalate has been detected in DI samples after some leaching steps. However, this technique cannot be used to analyze SW solutions because of the high concentration of anions and cations present in this media.
- Both alcohols and aldehydes in leachates have not been detected, and regarding gas samples, nor was CO (MDC < 3.5 ppm).

## Slide 13: WP5 Graphite – Overview of Main Outcomes
  CIEMAT, Enresa, ALD
VANDELLÓS I GRAPHITE COMPILATION REPORT: THERMAL DECONTAMINATION AND IGM WASTEFORM RESULTS
  The smallest amount of 14C in inert atmosphere obtained in is in contrast with the experiment performed with other graphite type reactors. The different behaviour can be explained by the loss of 14C of the graphite surface during reactor operation.
  More experiments with irradiated graphite will be programmed to optimise the decontamination factors (14C/12C) without significant mass lost starting from the valuable results obtained.
  The set of experimental data indicates that a lower treatment temperature and lower reactivity of the oxidant agent increase the 14C/12C ratio.
  The organic carbon has been found in deionized water as formate (HCOO-) an oxalate (COO2-)2
  Both alcohols and aldehydes in deionized water and granitic bentonite have not been detected at any time of the leaching process.
  CO were not found in the gas phase of the leaching process with a MDC (< 3.5 ppm), except for the first and second leaching period with granitic bentonite water (30.9 mg/l and 10.4 mg/l).
  The values obtained for 14C are lower than Minimum Detectable Activity.
  The Leaching rate (Rn) for 60Co and 137Cs in granitic bentonite water, decreases with the time and after 356 days it will be constant.
  The durability of the IGM glass matrix has been validated by leaching experiments.
  It is possible to close the pore system in the irradiated graphite without to increase the volume of the waste.

## Slide 14: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  - Forschungszentrum Jülich GmbH, Institute of Energy and Climate Research, Nuclear Waste Management and Reactor Safety (IEK-6), Jülich, Germany
  Title of report on CAST website
  - Final evaluation of leach rates of treated and untreated i‑graphite from the Rossendorf Research Reactor (D5.12)
  Key outcomes as presented in report
  - Inhomogeneous distribution of 14C in form of hot-spots, whereas most of 14C is concentrated in pores, probably, following its main precursor 14N;
- Most of 14C is released from RFR-graphite in form of 14CO2 along with a small fractions of CO or Corg;
- The 14C annual release rate of 5.2∙10-3 %/a, if encapsulated in cementitious material  meets WAC of Schacht Konrad (<1%) for maximum capacity of i-graphite;
- Thermal treatment of RFR-graphite is not considered to be an effective treatment step, as it separates only a minor fraction of 14C (i.e. ca. 8%) and generates unwanted secondary wastes.

## Slide 15: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  EDF R&D France (with participation of Andra and CEA)
  Title of report on CAST website
  Review on carbon 14 leaching data in French irradiated graphite (D5.1)
  Key outcomes as presented in report
  carbon 14 leaching rate is very slow as soon as a steady state leach rate is achieved after the elapse of around 100 to 200 days
  the main challenges for carbon 14 leaching studies in graphite is this very slow release rate. To obtain significant results (above the quantification limit) it is needed to use specific conditions (masses of samples - leachate sampling…)
  the results obtained on the radionuclides behaviour might depend on the history and on the background behind the used i-graphite. The results obtained on the French i-graphite cannot be directly and simply extended to other i-graphite.

## Slide 16: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  ANDRA DRD France (with participation of EDF and CEA)
  Title of report on CAST website
  Carbon-14 speciation in solution and gas from French graphite waste (D5.8)
  Key outcomes as presented in report
  An experimental methodology was specifically designed in order to increase carbon 14 release so as to identify the organic and inorganic released species
  more than 95% of the released carbon 14 was found in the liquid phase. After 100 to 200 days, the speciation of the released carbon 14 reaches a quasi-steady state to around 30% of the total carbon 14 released as organic species (liquid phase).
  The released carbon 14 in the gas phase samples is as a mixture of organic species and/or CO.
  Some parameters as the water chemistry and the specific surface area seem to have an impact on the results.

## Slide 17: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  - Lithuanian Energy Institute, Lithuania
  Title of report on CAST website
  - Report on modelling of C-14 inventory in RBMK reactor core (D5.17)
  Key outcomes as presented in report
  - The aim of this work was to perform the neutron activation modelling of Ignalina Nuclear Power Plant Unit 1 reactor RBMK-1500 graphite stack and (combining modelling results with the available C-14 activity measurement results) determine C-14 inventory. Key report outcomes:
  - Total C-14 activity in the graphite stack: 3.222×1014 Bq
  - Total mass of the graphite stack: 1.700×109 g (1700 t)
  - Average C-14 activity in the graphite stack: 1.895×105 Bq/g
  It should be noted that the above numbers are only for the reactor RBMK-1500 graphite stack consisting of GR-280 grade graphite blocks. The remaining graphite components in the reactor (graphite rings, sleeves, rods and other graphite parts in minor quantities) are not taken into account

## Slide 18: WP5 Graphite – Overview of Main Outcomes
  Name of Organization & Nationality
  Horia Hulubei National Institute for R&D in Physics and Nuclear
  Engineering (IFIN-HH)
  Title of report on CAST website
  REPORT ON THE RELEASE OF C-14 FROM IRRADIATED VVR-S
  GRAPHITE TO SOLUTION AND GAS PHASE
  Key outcomes as presented in report
  - the release of C-14 and H-3 into liquid and gas phase were performed over a 12 months period
  - the rate of release of C-14 and H-3 from i-graphite into liquid phase decreased to 130 Bq /day per kg, and respectively 10 Bq /day per kg after 12 months
  - the total C-14 and H-3 released from graphite samples and retained in solution represented approximately 2.271% and respectively 0.073% the initial estimated inventory
  - a major fraction of the total release occurs in the first months and a slower release on long time scale. However, these results should be applied cautiously for a long time prediction.

## Slide 19: With Thanks To:
Nelly Toulhoat,
Nathalie Moncoffre,
Ernestas Narkunas,
Povilas Poskas,
Crina Bucur,
Camelia Ichim,
Ionut Florea,
Relu Dobrin,
Liliana Bujoreanu,
Cristina Diaconescu,
Daniela Diaconu,
Laurent Petit,
Stephan Schumacher,
Stephane Catherin,
Mauro Capone
N. Cherubini,
A. Dodaro,
T. Guarcini
Natalia Shcherbina,
Andrey Bukaemskiy,
E. Petrova,
M. Guengoer,
Werner von Lensa,
Marina Rodríguez Alcalá,
Enrique Magro,
Eva María Márquez,
Gabriel Piña,
Johannes Fachinger,
Viorel Fugaru,
Borys Zlobenko,
Borys Shabalin,
Vadim Skripkin,
Yriy Fedorenko,
Victor Yatzenko,
Steve Williams.

## Slide 20: Radioactive Waste Management
Web:
www.gov.uk/rwm
Email:
GDFenquiries@nda.gov.uk
rwmfeedback@nda.gov.uk
Simon.Norris@nda.gov.uk