## Slide 1: CAST Expert Review Group Findings
Irka Hajdas (ETHZ)
Fraser King (Integrity Corrosion Consulting Ltd)

## Slide 2: Contents
Introduction to the CAST Review Group
Comments on analytical method development aspects of CAST
  Irka Hajdas
Comments on experimental programmes and performance assessments aspects of CAST
  Fraser King

## Slide 3: CAST Advisory Group
Make-up of CAST Advisory Group
  CAST Coordinator
    Simon Norris (Steve Williams)
  WP Leaders
    WP2 Jens Mibus
    WP3 Sophia Necib
    WP4 Pascel Reiller
    WP5 Simon Norris
    WP6 Manual Capouet
    WP7 Erika Neeft
  External members
    Irka Hajdas (background in carbon-14 analysis and measurement)
    Fraser King (background in corrosion)
  Secretariat
    Ally Clark (Ellie Scourse)
Functions of CAST Advisory Group
  General project oversight
  Annual review by external experts

## Slide 4: CAST Objectives
CAST project objectives
  “…. to gain new scientific understanding of the rate of release … under geological disposal conditions …, its speciation and how these relate to carbon-14 inventory ….”
  “These results will be evaluated in the context of national safety assessments and disseminated to interested stakeholders”
  “The new understanding should be of relevance to national safety assessment stakeholders ….”
  “…. and will also provide an opportunity for training for early career researchers.”

## Slide 5: Review of CAST Project Carbon-14 Analytical Developments
Irka Hajdas
ETHZ, Zurich

## Slide 7: Review of CAST Project Experimental and Performance Assessment WPs
Fraser King
Integrity Corrosion Consulting Ltd, Canada

## Slide 8: Context for review of CAST experimental WPs
Inventory
  How much?
  In what (chemical) form?
  How is it distributed?
Release
  Rate
  Mechanism
  Speciation
Transport/reaction
  After release
  Possibility of change of speciation
  Out of scope?

## Slide 9: WP2 Steels
Aims
  State-of-the-art review
  Advance understanding of C-14 speciation
  Develop analytical techniques
  Measure release rates
  Confirm/measure inventory
Challenges
  Obtaining and working with irradiated samples
  Extremely low C-14 release rates in test environments
  Measuring corrosion rates of irradiated materials under alkaline conditions
  Demonstrating congruent release of C-14
  Distinguishing surface contamination from IRF from long-term release
  Uncertainty in inventory, in part because of lack of archive material (actual N content)
  Effect of dose rate on release and speciation of C-14
  Duration of experiments
  Characterisation of inventory – how much, in what form, and distribution within samples

## Slide 10: Summary release of 12C and 14C
Organi-sation | Condi-tions | Material | Liquid phase |  | Gas phase | 
 |  |  | Spec. | % | Spec. | %
PSI inactive | alkaline anoxic | SS | AA, FA, OA | 95 | Met, Eth | 5
PSI active | alkaline anoxic | SS | FA, AA, LA | n.d. | n.d. | n.d.
NRJ/ Wood | alkaline anoxic | SS | CO3 | 90 | Met, (CO) | 10
KIT | acidic digestion | SS | organic | 70 | organic | 30
SCK | alkaline anoxic | CS | AA, FA | n.d. | Met | n.d.
Ciemat | alkaline oxic | SS | n.d. | n.d. | CO | n.d.
 | acidic oxic | SS | OA | n.d. | CO | n.d.

## Slide 11: WP2 Steels
Achievements/highlights
  Obtaining samples and making C-14 measurements on activated materials
  Improved understanding of release of C-14
  Microstructural characterisation of irradiated material
    Where is C-14 located and in what form?
  Improved understanding of inventory
  Good understanding of rate of corrosion under disposal conditions (inactive samples)
  Issue of congruent release
Release of C-14 from two irradiated SS samples in alkaline anoxic solution and one blank (Visser-Týnová et al., CAST Report D2.8)
Microstructure irradiated JRQ carbon steel (Druyts et al., CAST Report D2.7)

## Slide 12: WP3 Zircaloys
Aims
  State-of-the-art review
  Advance understanding of C-14 speciation
  Develop analytical techniques
  Measure release rates
  Confirm/measure inventory
Challenges
  Obtaining and working with irradiated samples
  Extremely low C-14 release rates in test environments
  Measuring corrosion rates of irradiated materials under alkaline conditions
  Demonstrating congruent release of C-14
  Uncertainty in inventory, in part because of lack of archive material (actual N content)
  Effect of dose rate on release and speciation of C-14
  Duration of experiments
  Characterisation of inventory – how much, in what form, and distribution within samples
  Influence of hydride layer
  Possibility of change in corrosion/release rate as oxide thickens

## Slide 13: C-14 analyses
Organisations | Speciation |  |  |  | Method
 | Solutions | Organics | Inorganics | Gas | 
CEA | NaOH | Glycolate Acetate Formate Oxalate | Carbonate |  | Anionic Chromatography
 | Blank | Acetate Formate | Carbonate |  | Anionic Chromatography
SCK.CEN | Ca(OH)2 | Acetate Formate |  | Methane Ethene CO2 | Ion Chromatography Gas Chromatography
SUBATECH | NaOH | Formate Acetate Propionate Oxalate |  |  | Ion Chromatography
Zr type does not influence C-14 speciation (Zr-4 + M5TM)
Some differences for CEA + SUBATECH => Difficulty of the analyses
Liquid phase=> Carboxylic acids + Carbonates
Gas phase => Hydrocarbons + CO2

## Slide 14: Corrosion rate measurements
Organisations |  | Corrosion rate (nm/yr) |  |  |  |  | 
 | Materials | Durations | Unirradiated |  | Durations | Irradiated | 
Methods |  |  | H2 meas. | Electrochemistry |  | C-14 leaching fraction | Electrochemistry
RATEN ICN | Zr-4 (CANDU) Oxidised As-received Cut at one end | 12mths |  | 0.3 110 60 | 6 mths 18 mths |  | 110 50
RWMC | Zr-2 | 2 yrs | ~5 |  | 6.5 yrs | ~ 1 | 
SCK.CEN | Zr-4 |  |  |  | 6 mths | 84 | 
=> Decrease of the CR with time
Influence of irradiation on the CR
Significant uncertainties on the measurements (various techniques,…)

## Slide 15: WP3 Zircaloys
Achievements/highlights
  Obtaining samples and making C-14 measurements on activated materials
  Good agreement between measured and calculated inventories
  Good database of long-term corrosion rates
  Unclear whether C-14 released congruently
  Less C-14 in oxide (7.5%) than currently assumed as IRF in PA
Comparison of irradiated (assuming congruent C-14 release) and inactive corrosion rates of Zircaloy (Herm et al., CAST Report D3.15)
Electrochemical behaviour of Zy-4 after 6, 8, 12 months (Bucur et al., CAST Report D3.16)

## Slide 16: WP4 Spent Ion Exchange Resins
Aims
  State-of-the-art review
  Understanding inventory and speciation
  Determining release rate and mechanism
Challenges
  Wide range of SIER characteristics due to different types of operating plants and different IX locations within a given plant
  Relating release to geological disposal conditions for cemented and immobilised SIERs
    Effects of porosity, groundwater flow, etc.
  Uncertainty over long-term (radiation) stability of resins
Rizzo et al., CAST Report D4.5, Appendix V

## Slide 17: WP4 Spent Ion Exchange Resins
Achievements/highlights
  Because of the wide variability of SIERS, country-specific inventories and speciation are required
  Good understanding of speciation
    In general, majority present as inorganic C-14 but fraction depends on reactor type
      PWR: 1-70% organic
      BWR: 1-5% organic
      CANDU: 7% organic (single sample)
  Gas-phase inorganic C-14 is released under conditions that simulate storage and long-term disposal (alkaline pH)
  Effect of immobilization in cement, epoxy, bitumen matrix
    At least for cement, significantly reduces release of C-14

## Slide 18: WP5 Irradiated Graphite
Aims
  Build on earlier Carbowaste project
  Determine inventory and distribution of C-14 and factors that may control these
  Measure rate and speciation of gaseous and dissolved C-14 released
  Assess impacts of selected waste treatment options
Challenges
  Diversity of national interests
    Amount of i-graphite waste
    Surface vs. deep geological disposal

## Slide 19: WP5 Irradiated Graphite
Achievements/highlights
  Detailed understanding of distribution of C-14 within the waste
  Improved mechanistic understanding
    Small releasable fraction
    Initial fast release, slow long-term
    Speciation
    Inventory and especially distribution
    Consequences of in-reactor behaviour
Graphite leaching tests at RATEN ICN, Toulhaut et al., CAST Report D5.19
C-14 release mechanism proposed by RWM, Toulhaut et al., CAST Report D5.19
ENEA exfoliation studies, Toulhaut et al., CAST Report D5.19
Impact of in-reactor irradiation and temperature, Toulhaut et al., CAST Report D5.19
C-14 leaching kinetics determined by FZJ, Toulhaut et al., CAST Report D5.19

## Slide 20: WP6 Relevance to the Safety Case
Aims
  Improve treatment of C-14 in safety analysis/ assessment
    Speciation, IRF, release rate, etc.
  Improve treatment of C-14 in safety case
    Scientific understanding
Challenges
  How to influence experimental groups to study processes that are safety-relevant
  Diversity of national disposal programmes
  Abstraction of data (and uncertainties) from experimental programmes

## Slide 21: WP6 Relevance to the Safety Case
Achievements/highlights
  Understanding of relative importance of C-14 for different host rock types
    Clay vs. crystalline vs. salt
  Understanding of relative importance of C-14 for different waste types
    E.g., for spent fuel, C-14 will likely decay in long-lived canister
  Understanding of relative importance of C-14 depending on repository location
    Surface vs. deep disposal
  CAST has produced much useful information for the safety case as well as for the safety analysis

## Slide 22: WP6 Relevance to the Safety Case (M. Capouet, presentation WP6 technical meeting Davos, September 2017, verbatim transcript with FK emphasis)
Clay host rock
  In terms of influence (PCC) : IRF < Congruent release << Kd_concrete << Kd_clay_rock (Ondraf/Niras, Nagra, NRG/COVRA).
  Impact of IRF is less pronounced. Only a factor 5 in case of low corrosion rates (Nagra).
  Diffusion through the clay barrier remains the key processes to attenuate the dose rate (even if Kd=0).
  Near field sorption (cement) has little impact.
  Advective (gas) scenario is the most impacting.
  Far Field (clay layer of a few tens of meters thick) has impact from Kd ~ 1E-04 m3/kg in a diffusion scenario (reference scenario).
  For some disposal systems/programs, conservative modelling of C-14 source terms assuming 100% IRF is possible. Considering a conservative diffusion in a clay rock of a few tens of meters thick leads to a C-14 decay in the disposal system of a factor 500.

## Slide 23: WP6 Relevance to the Safety Case (M. Capouet, presentation WP6 technical meeting Davos, September 2017, verbatim transcript with FK emphasis)
Crystalline host rock
  SIERs
    Not a barrier.
    The conditioning matrix limits the water flow :
      Source term release governed by the cement evolution through time dependent diffusion coefficients and hydraulic conductivities [Fortum, SKB].
      The epoxy matrix provides a retardation capacity [Andra].
    Sensitivity analysis with Kd [1E-5 – 1E-3] m3/Kg : Low Kd (Host formation and cement) shows an impact (one order of magnitude)
  SIERs [Fortum]
    SA calculation performed assuming 15% C14 is organic (measurements on VVER).
      Are we really conservative considering large variabilities in SIERs inventory ?
  IRF influences more the radiological impact (than in clay systems). In current SA:
    Activated metals:
      IRF=0 is still OK ?
    Zircaloy
      IRF=20%; Lowering IRF could attenuate radiological impact.
  Transport in crystalline rock in form of soluble or gaseous form (transport in either form does not influence much the impact)

## Slide 24: WP6 Relevance to the Safety Case (M. Capouet, presentation WP6 technical meeting Davos, September 2017, verbatim transcript with FK emphasis)
Salt host rock
Reference case : No release.
Altered evolutions :
  Container defects at initial and later times.
  Gas transport.
IRF_Zircaloy (not reprocessed) assumed to be released as CO2 (unsaturated).
CAST experimental conditions (in solution) not suitable for Salt:
  IRF based on First Nuclides results (IRF<1%).
C-14 radiotoxicity depends on IRF in volatile form and evolving porosity.
Assumption of initial defect containers critical for the C-14 release; After a few hundreds years=> porosity is close and C-14 release is stopped.
The highest priority to reduce the uncertainty on the release behaviour of C‑14 is mainly related to three questions:
  Is water necessary to transfer C‑14 into volatile form or does this occur also without the presence of humidity?
  What is the percentage of C‑14 which can be released into volatile form?
  What is the temporal behaviour of the release?

## Slide 25: Reduction of conservatism
LEI - release from irradiated graphite

## Slide 26: Conclusions
“… to gain new scientific understanding ….”
  Clearly achieved
“…. of relevance to safety assessment …”
  Useful data generated for safety analysis and especially underlying information to support the safety case
“… disseminated to stakeholders ….”
  Workshops, impressive number of reports/ deliverables, this symposium, RDC special edition, …
“… opportunity for early career researchers ...”
  Look around the audience